NEW THEORY AND TECHNICS IN BORING

# Hu Guoqing, Luo Renfei

Department of Mechanical and Electrical Engineering,

Xiamen(Amoy) University, China

### ABSTRACT

This paper has four main contents: a lot of experiments prove that the cutting solution of as mineral oil and a rectangular wave cutting feed are optimum methods for boring polymethylmethacrylate; the flow and temperature field profile of the cutting solution in the chute of the fluted twist drills are studied mathematically; the theoretical formula of the cutting friction coefficient and the viscosity (μ) of the cutting solution are deduced mathematically; the theoretical formula for surface roughness (Ra) in boring is derived mathematically.

#### INTRODUCTION

A transparent observation window (Hu, 1992) must be used when Laser Doppler Anemometry (LDA)is used to measure the flow field profile of the flow path of a hydraulic valve. The common hot working process when optical glass is employed fails to meet the machining demands. Only by employing machined polymethylmethacrylate can the demands of the flow path be obtained. However polymethylmethacrylate machining has many influencing factors, for example: cutting heat, cutting thickness, etc. which can result in a glutinous and a very poorly transparent working surface, which is not suitable for using LDA to measure the distributions of the flow fields of the flow path of a hydraulic valve. So far, few papers reported on the distribution of the flow and temperature field profile of the cutting solution in fluted twist drill's cutting chutes and on the theoretical formulae of the roughness of surface of boring based on the viscosity (μ) of the cutting fluid etc. This paper aims to analyze and probe these problems.

1. BORING PROCESS

In order to obtain the flow path for a polymethylmethacrylate surface with a low surface roughness and high machining precision transparent surface, the authors have done a series of experiments as follows:

(1) high-speed-drilling, low-cutting-feed: fail

(2) high-speed-drilling, fast-cutting-feed: fail

Analyzing the failure in experiments (1) and (2): The roughness of surface is decreased when boring is done at high speed cutting based on theory, but the roughness of surface is increased when a helical working-surface is formed in quick cutting. That is one of the fail factors of the experiments.

From the experiments(1) and (2), a very high temperature on the working surface is engendered at high-speed-cutting(papers (Hu, 1992), (CGMM, 1978), (Lu, 1985), (Cheng, 1985), (Guo, 1984), (BUAA and NPU, 1984) above 1000, meaning that the polymethylmethacrylate can be molten. So charring, black cutting scrapes and a glutinous working surface appear.

Grinding can eliminate the charred working surface, but polymethylmethacrylate is subject to being scratched and forms a poor reflecting surface. Hence, it is no use in LDA measurement; and experiments (1) and (2) fail.

(3) low-speed-drilling, fast-cutting-feed, fail.

(4) low-speed-drilling, low-cutting-feed, fail.

Analyzing the failure in experiments (3) and (4): First, the low-speed-drilling is required because it produces a small cutting heat and prevents polymethylmethacrylate charring. When low-speed-drilling and a fast cutting-feed are adopted the helical and special roughness working surface is formed. Sometime low-speed-drilling and low-cutting-feed also produces the problem of high surface roughness (Hu, 1993(a,b)), (CGMM, 1978), (Lu, 1985), (Cheng, 1985), (Guo, 1984), (BUAA and NPU, 1984). Although the charring of polymethylmethacrylate the working surface at low-speed-cutting is not so bad as at high-speed-cutting, the working surface is very rough (Ra>100). Therefore, such a working surface is no good for use in the LDA to measure.(5) Using the organic solvent grinding process method can solve the problem of the rough-working-surface, because the organic solvent grinding process can be regarded as being a great many micro-cutting lips. However, being a liquid, it is impossible that the organic solvent makes the convexity of rough surface cut and the concavity of rough surface not cut in fig.1. As time goes on, this method makes convex surface feature more convex and the concave more concave. Even if a grinding tool is used to polish the convex surface, the surface never meet the demands for optical measurement. So, the experiment (5) fails.

Fig.1 Organic solvent working surface

organic solvent

convex surface

concave surface.

(6) Cold water is used as a cutting solution, we have done experiments (1) to (4), respectively, the transparency of the working surface is better than in experiments (1) to (4), respectively, but it does not accord with the requirement. So experiment (6) is a failure.

(7) Soapy water is used as cutting solution, we have done the experiments (1) to (4), respectively. We can find that the experiment results are better than that in experiment (6), but not good enough to accord with the demand. So experiment (7) is a failure.

We can obtain a useful result when we analyze the failure factors of experiments (6) and (7) respectively. Air is a natural cold cutting solution, and the viscosity of cutting solution is one of the main factors to reduce the roughness of the surface.

(8) Mineral oil is used as a cutting solution. A high precision surface with low roughness results of high-speed-drilling with a low cutting-feed, when we have done the experiments (1) to (4), respectively. Numerous experiments have proven that high-speed-drilling with rectangular wave cutting feed is an optimum boring method to machine polymethylmethacrylate. Using method produce a higher machined precision surface and a lower surface roughness than continuous cutting feed, and accords with the demands of a surface for LDA measurement.

The machining method of experiment (8) involves theoretical analysis: the viscosity of the cutting solution has an important effect on surface roughness in boring. The greater is viscosity, the lower is the surface roughness of the worked surface, but it is a non-linear relationship. When the viscosity is at the upper limit, the roughness of surface of working surface is increased again as in figure 2, if the viscosity keeps increasing (solid lubricant is used in experiment).

The more viscosity is (over the superior limit), the worse diffuse of heat is. A high temperature region is easily made on the cutting surface, which makes it difficult for the cutting chips to be discarded, resulting a high roughness on the working surfaces.

Viscosity forms a protective film on the surface of the cutting lip as in fig.3.

Fig.3 Fluted drill twist cutting lip

The protective film can protect the cutting lip from direct contact with the working surface during the cutting processing in boring. Air, cold water, soapy water and mineral oil etc. produce a different thicknesses of protective films. Air can not form a protective film; water makes a very thin and easily volatilizable protective film; mineral oil produces a very thick film which is not easily ruined. Hence, mineral oil is selected for the cutting solution in boring polymethylmethacrylate, for it produces a higher machining precision surface and lower roughness than air and water. Experiment show that the ruined protectiive film of the surface of the cutting lip in the process of the rectangular wave cutting-in is complemented with the machining cutting-out (fig.4,5). Therefore a certain degree of thickness of protective film is always on the surface of the cutting lip. Such a protective film can reduce the boring friction force, improve cutting life, and protect the cutting lip from contacting directly with the working surface.

A high precision and low roughness of the working surface is obtained through the adoption of such boring parameters. That reason that high-speed-drilling can improve the precision of the surface and reduce the roughness can be explained as follows. Polymethylmethacrylate is a plastic material. Low speed drill makes it easy for the cuttings chips to stick on the surface of the cutting lip and the working surface, hence increasing the cutting friction force. High speed drilling, on the other hand, prevents the cutting chips from sticking on the surface of the cutting lip and the working surface, and decreases the cutting friction force. The experiment has shown that increasing the cutting-speed to reduce the surface of roughness (fig.6) is not pronounced when the cutting speed is greater than the limit cutting speed. The experiment has also shown that improving the cutting-speed to increase the temperature of working surface is not pronounced when the cutting speed is greater than the limit cutting speed as in fig.7.

| Fig.6 Ra depends on the cutting velocity V | Fig.7 The cutting temperature(T) depends on velocity V |
| --- | --- |

2. THE FLUID KINEMATICS ANALYSIS’S OF FLUTED TWIST DRILL'S CUTTING CHUTE

The fluid in the fluted twist drill's cutting chute is Newtonian fluid, which corresponds to the fundamental assumption of Naiver-Stokes. We can define the viscosity fluid continuity and Naiver-Stokes equation in a Cylindrical Coordinate System in fig.8 and fig.9 as follows:

(1) Continuity equation:

¶Vr¶r+1r¶Vq¶q+¶Vz¶z+Vrr=0								(1)

(2) Naiver-Stokes equation:

¶Vr¶t+Vr¶Vr¶r+Vqr¶Vr¶q+Vz¶Vr¶z−Vq2r=fr−1ρ¶p¶r+ν(Ñ2Vr−Vrr2−2r2¶Vq¶q)	(2)

¶Vq¶t+Vr¶Vq¶r+Vqr¶Vq¶q+Vz¶Vq¶z+VrVqr=fq−1ρr¶p¶q+ν(Ñ2Vq+2r2¶Vr¶q−Vqr2)	(3)

¶Vz¶t+Vr¶Vz¶r+Vqr¶Vz¶q+Vz¶Vz¶z=fz−1ρ¶p¶z+νÑ2Vz				(4)

a) Head of fluted drill twist			b) Cylindrical coordinate system

Fig.8 Fluted drill twist

Fig.9 The cross-section of fluted drill twist

The fluid movement in the cutting chute of a fluted twist drill is very complex; the use of three- dimensional fluid flow for analyzing the cutting condition is very difficult. So, an assumption is made from the actual conditions as follows: (1) No cutting chips, but cutting the solution is drained off in the fluted drill's cutting chute during the boring; (2) the flow is homogeneous independent of time, in the cutting chute of the fluted twist drill, so that the flow field can be regarded as homogeneous flow; Vr in the cutting chute of the fluted twist drill can be considered to be very small, thus Vr»0,Vq>>VrVz>>Vrand¶¶z=0, the weight function f can be omitted. So the equations (1) to (4)are simplified respectively as follows:

Continuity equation

∂Vz∂z=0											(5)

Naiver-Stokes equation:

−Vθ2r=−1ρ∂p∂r										(6)

Vz∂Vθ∂z=ν(∂2Vθ∂r2+∂2Vθ∂z2+1r∂Vθ∂r−Vθr2)						(7)

Vz∂Vz∂z=−1ρ∂p∂z+ν(∂2Vz∂r2+∂2Vz∂z2+1r∂Vz∂r)					(8)

If: Vq>>Vz,¶2Vz¶r2>>¶2Vz¶z2,¶Vq¶r>>¶Vq¶z

so, (7) can be simplified:

d2Vqdr2+1rdVqdr−Vqr2=0								(9)

The solution of (9) can be obtained:

Vθ=C11r+C2r										(10)

the boundary condition substitutes r=r1Vq=wr1into(10):

Solves the equation (10) and obtain: , so:

Vθ=ωr											(11)

Formula (11) is substituted into (6) and obtains:

p=12ρω2r2+C1									(12)

We know that ∂P∂zis a constant from (12), otherwise, we can assume that the pressure drop per unit length at the z-direction is substituted into (8) and obtains

∂2Vz∂r2+1r∂Vz∂r=C0μ									(13)

The solution formula of (13) obtains:

Vz=C04μr2+C1lnr+C2								(14)

The boundary condition is

r=r1 Vz=0 into (14)

Vz=C0r24μ2+4μVm−C0(r22−r12)4μlnr2r1lnr+C04μr12+4μVm−C0(r22−r12)4μlnr2r1lnr1	(15)

assume:

a=4μVm−Co(r22−r12)4μln(r2r1)lnr1

Thus formula (15) can be simplified:

Vz=C04mr2+alnr+b									(16)

The compound moving trace of the velocity Vz and Vr is just a helix line of the cutting chute of the flute twist drill, so the theoretical study is corrected.

3. THE STUDY OF TEMPERATURE PROFILE OF THE FLUID IN THE CUTTING CHUTE OF THE FLUTED TWIST DRILL

From the energy conservation law (Liang, 1982)

DDt(e+V22)=2mρeijeij−λρ¶¶xj(¶T¶xj)							(17)

As the cutting temperature is very high, the kinetic energy 12V2 of the cutting solution is relatively very small and 12V2 can be omitted. The energy of distortion is also very small, so 2ρei,jei,j can be omitted. Assuming that the specific heat capacity at constant volume is Cv, thus e=CvT, then (17) can be simplified as follows:

Vx∂T∂x+Vy∂T∂y+Vz∂T∂z=−λρCv(∂2T∂x2+∂2T∂y2+∂2T∂z2)			(18)

We can change the Cartesian Coordinate System into a Cylindrical Coordinate System as follows:

x=rcosq

y=rsinq

Vx=Vrcosθ−Vθsinθ=−ωrsinθ

Vy=Vrsinθ+Vθcosθ=ωrcosθ

and ¶¶q=0 is considered not to be changing, hence:

∂T∂x=∂T∂rcosθ

So the (18) can be changed as follows:

λρCv(¶2T¶r2+1r¶T¶r+¶2T¶z2)+Vz¶T¶z=0							(19)

As the diameter of the fluted twist drill is very small, we can assume that the heat in the Z-directional is dominant and Vz can be derived from VA (VAis mean velocity in the r-directional). So

¶T¶r=0and¶2T¶r2=0

Formula (19) can be developed:

T=-λρCvVAC1e−ρCvVAλz+C2								(20)

boundary condition (Hu, 1993, CGMM, 1978)

z=0,T0=C0V0.3S0.15t0.08

C0: constant

V:  cutting speed =Dn/6000 (m/s)

S:  cutting seed displacement;

t:  length of cutting;

If z approaches infinity, T=T¥=constant, thus (20) can be rewritten as fellows:

T=(T0−T∞)e−ρCVVAλz+T∞								(21)

4. FRICTION FORCE ANALYSIS’S OF OIL FILEM

Fig.11 is a oil film of a fluted twist drill, we can derive the velocity formula (Pian, 1986) as follows:

Fig.10 The theoretical curve of the cutting solution	Fig.11 Oil film cross-section of fluted twist

temperature is depended on the displacement.				drill.

Vq=-r02(r0+d)2−r02wr+r02(r0+d)2(r0+d)2−r02wr					(22)

As: ro>>d,d2 can be omitted so that (22) can be simplified as follow:

Vq=r02dw[−r+r0(r0+2d)1r] 								(23)

From the generalized Newton Shear Stress Law:

Prq=m(¶Vq¶r−Vqr)=-mr02dwr2(r0+2d)						(24)

on the working-surface, that r=r+d.

Prq=-mr02dw(r0+2d)(r0+d)2=-mwr0d							(25)

the Force in per unit area is:

F=-mwr0d=-mV0d									(26)

the sum of the friction force in boring is:

f=f'+F=f'−wmr0d=f'−wmdr0=f'−mV0d						(27)

f' is dry friction force. The total boring friction force decreases as the viscosity of the cutting solution increases from the formula (27). (27) is a theoretical formula showing that the roughness of the surface depends on the viscosity of the cutting solution. If the viscosity of the cutting solution is greatens the limit, the friction force increases in the adverse direction, and accordingly, raises the roughness of the surface again as in fig.12. Fig.12 correspondes to the experiment curve in fig.2. From fig.12, the viscosity of cutting solution is a best viscosity, but it is very difficult to find it. So a roughness surface always results from machining.

Fig.12 The theoretical curve of cutting         Fig.13 The theoretical curve Ra depend on V and 

friction and viscosity coefficient.

5. THEORETICAL ANALYSIS OF SURFACE ROUGHNESS

A gap h exists between the surface of the fluted twist drill and the working surface in boring, so the fundamental equation of the fluid moving in the gap is used for analysis. The Reynolds equation (Zhou et al., 1990, Chen et al., 1991) in the gap is as follows:

ddx(h3dpdx)=6Vmdhdx									(28)

The mean height is  in the gap and Ra is the surface roughness. Substituting h= +Ra into (28):

3(d+Ra)2dRadxdpdx+(d+Ra)3d2pdx2=6VmdRadx				(29)

Assumption that Ra is independent of dpdx=M and d2pdx2=Nand substitute into (29):

−3MNln(Ra+d)−3VmN1(d+Ra)2=x+c						(30)

Substitute boundary condition: x=0 and Ra=0 into (30):

c=-3ABlnh−3VBm1h2

So (30) can be changed as follows:

MN[Rad+o(Rad)2]+VmNd2[−2(Rad)+o(Rad)2]=-x3				(31)

As Kh >>Ra. the high order infinitesimal can be omitted in (31)

Ra=xd3N3(2Vm−Md2)									(32)

The mean surface roughness in boring can be derived from:

Ra=12πR02πRRadx=πRNδ33(2Vμ−Mδ2)						(33)

The mean surface roughness (Ra) can be derived in (33). (33) is also a theoretical formula for the roughness of surface Ra in boring. The roughness of surface (Ra) can be assessed predictably before boring from in Fig.13, so the theoretical curve Ra depends on V and . This conclusion is the same as the formula (27).

6. CONCLUSION

(1) A rectangular wave cutting feed method is proposed in boring process, and mineral oil is selected as the optimum type of cutting solution.

(2) The kinematic character of the cutting solution in the cutting chute of the fluted twist drill is analyzed and the mathematical formula of movement of the cutting solution is derived from.

(3) The temperature profile of the cutting solution in the cutting chute of the fluted twist drill is analyzed and a mathematical formula of the movement of the cutting solution is derived. Such mathematical formulae have a very important role in theory and practices when studying diffusive heat of the cutting solution.

(4) The relation of theoretical formula and the viscosity of the cutting solution is derived from the mathematics, which is very important for obtaining high precision and low surface roughness in boring, and in guidance for selecting the optimum cutting solution.

(5) The theoretical formula of surface roughness in boring is derived from the Reynolds equation in the gap, which is very important in theory and practice when selecting a economical and reasonable cutting solution.

#### REFERENCES

- Chen Bei-Xian et al, Fluid Lubricant theory and Application, Mechanical Engineering Press, 1991.

- Cheng Ri-Qu, Theory of Metal Cutting, Mechanical Engineering press, 1985.

- Co-compiler of Beijing University of Aeronautics and Astronauts and Northwestern Polytechnical University, Metal Tectonics, National Defense Engineering Press, 1984.

- Compiler Group of Machine Manufacturing, The Fundamental of Manufacturing, People's Education Press, 1978.

- Guo Weipong, Metal cutting Machine tool, Mechanical Engineering Press, 1984.

- Hu Guoqing, The study of energy dissipation of hydraulic valve's flows path, Ph.D. Thesis. CUST, CHINA, 1993(a).

- Hu Guoqing, A Study on the New Machining Process in Boring and the Theoretical Analysis of Surface Roughness. International Conference on Machining Technology, Guangzhou China, 1993(b), pp.133-136.

- Hu Guoqing, Boring in Polymethylmethacrylate and Fluid Mechanics Relationship of Surface Roughness with Cutting Fluid, Journal of Chengdu University of Science and Technology, 1994, No.1, pp.53-56

- Hu Guoqing, Study on the temperature fields of the fluid in the fluted twisted drill’s chute and its film friction, Journal of the Chinese Modern Machinery, 1996, Vol.4 pp.20-22.

- Liang Yunqi, Fundamental of heat transfer and distortion in Machine Manufacturing, Mechanical Engineering Press, 1982.

- Lu Duiqian, Metal Cutting-tool, Mechanical Engineering Press, 1985.

- Pian Wenquan, Fluid Mechanical Fundamental, Mechanical Engineering Press, 1986.

- Zhou Zhuru et al, Fluid Lubricant Theory, Zhejiang University Press, 1990.

Поступила в редакцию 29 августа 1999 года.