TAGUCHI ANALYSIS OF POLYMER CONCRETE MECHANICAL PROPERTIES

A.J.M.Ferreira, P.P.Camanho, M.Cristina Fernandes, M.A.V.Figueiredo, A.A.Fernandes

Instituto de Engenharia Mecânica e Gestão Industrial

Faculdade de Engenharia da Universidade do Porto

Rua dos Bragas, 4050-123 Porto Codex

PORTUGAL

# ABSTRACT

Polymer concrete is a relatively new concrete with a resin binder. These concretes aim to produce high-performance structures with high mechanical and corrosion-resistance properties. In this paper the results of three-point bending tests are discussed. The Taguchi method was applied, to plan the experimental programme and identity possible correlations and interactions among the mechanical behaviour controlling parameters.

- INTRODUCTION

Polymer concrete is a relatively new kind of concrete where a resin system binds together natural aggregates, such as silica sand. It is produced by mixing a liquid thermoset resin with inorganic aggregates (such as gravel, sand and fly ash). Initiators and promoters are added to the resin prior to its mixing with the inorganic aggregates to initiate the curing reaction. Polymer concrete therefore consists of well-graded inorganic aggregates bonded together by a resin binder instead of the water and cement binder typically used in normal cement concrete [1]. Typical resins used are polyester, epoxy ot methacrilate thermoset resins. The most common type of binder utilized in polymer concrete is unsaturated polyester because of its good properties and relatively low cost.

The advantages of polymer concrete are its very good strength, very good durability (e.g., freeze-thaw, acid, and abrasion resistance), very low permeability, and very fast curing time (polymer concrete cures in a few minutes or hours while portland cement concrete cures in a few days or weeks). The use of polymer concrete materials is growing very rapidly in many structural precast applications such as utility components (e.g., drains for acid wastes, undergound vaults and junction boxes, sewer pipes, power line transmission poles), transportation-related components (e.g., median barriers, bridge panels, railroad ties), and building panels [2].

The good strength and durability properties of polymer concrete allow the production of high quality precast components with very thin cross sections and low cover depths (in reinforced concrete), thus reducing dead loads in structures and minimizing transportation and erection costs. The very fast cure time of polymer concrete enables the rapid and efficient use of forms and other production facilities and confers to the structures higher resistance to large stresses due to transportation and erection operations.

Like portland cement concrete, polymer concrete has relatively low tensile strength compared to its compressive strength. Therefore, sudden and brittle failures occur in planes where tensile stresses exceed the tensile strength of the material. Reinforcing steel or FRP (fiber reinforced plastic) rods are therefore added in tensile zones of polymer concrete to increase its strength capacity, ductility and toughness
[3-6]. The objective of this paper is to report an experimental programme on polymer concrete, designed using Taguchi method [7-11].

- EXPERIMENTAL SET-UP

The samples were produced in prismatic shapes of 16x4x4cm for bending tests (figure 1).

Figure 1. Prismatic samples tested in three-point bending.

The experimental plan was prepared according to Taguchi method [7-11]. Five fabrication factors at two levels were chosen. The number of potential combinations, for this case would be costly. The Taguchi method reduces the number of tests to be performed, by the use of pre-set orthogonal arrays, without the loss of relevant information. Interactions among factors can be identified through the application of this method. Table 1 illustrates factors and levels selected. Table 2 shows the experimental plan devised.

Table 1.

Factors and levels (% in weight).

|  | FACTORS |  |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  | Type of resin | Additives | Resin content | Type of sand | Post-cure |
| Level 1 | Polyester | No | 17% | Clean sand | No |
| Level 2 | Epoxy | 25% | 20% | Foundry sand | Yes |

The selected array was L16 [7-11]. This array has 16 lines, corresponding to 16 tests performed. This array allows the evaluation of major effects of the factors on performance and the interaction between factors.

For each combination of factors, indicated in table 2, three tests were performed in a total of 48 tests.

Table 2.

Experimental plan, L16 (215).

- DISCUSSION OF RESULTS

Figure 2 displays a typical load-displacement curve resulting from the flexural test of polymer concrete beams.

Figure 2. A typical load-displacement curve for polymer concrete beams under flexural tests.

The results indicated in table 3, represent the average responses of the tests carried out (three tests for each combination), measured by three different parameters: maximum load, flexural strength, and flexural toughness.

Table 3.

Main results for three-point bending tests.

|  | Max Load | Flexural Strength | Flexural toughness |
| --- | --- | --- | --- |
| Test | [N] | [MPa] | [N.mm] |
| 2 | 2467.4 | 5.8 | 730.3 |
| 9 | 4240.4 | 9.9 | 1301.6 |
| 1 | 4273.2 | 10.0 | 1427.5 |
| 11 | 4356.3 | 10.2 | 2274.0 |
| 4 | 5182.2 | 12.1 | 1581.7 |
| 3 | 5491.5 | 12.9 | 1780.4 |
| 7 | 6323.6 | 14.8 | 1828.9 |
| 13 | 7050.0 | 16.5 | 1656.7 |
| 12 | 7229.8 | 16.9 | 4329.0 |
| 10 | 7881.1 | 18.5 | 2522.4 |
| 5 | 10335.9 | 24.2 | 2750.0 |
| 15 | 12052.3 | 28.2 | 3818.1 |
| 6 | 14406.6 | 33.8 | 5018.8 |
| 8 | 14689.4 | 34.4 | 4707.4 |
| 16 | 17439.7 | 40.9 | 6511.3 |
| 14 | 17893.3 | 41.9 | 6888.2 |

A statistical analysis (ANOVA) of the results was performed in order to evaluate the effects of the main factors and identify potential interactions between factors.

Table 4 shows the results of the ANOVA analysis: 5% significance tests were carried out. The contributions of the different factors to the response total variance are illustrated.

The study of table 4 shows that the main contributing factors to behaviour of the polymer concrete as measured by different response parameters are as follows:	Strength: charge (56.8%), type of sand (17.8%) and type of resin (3.6%). A significant interaction between charge and type of sand was observed (9.5%)

Toughness: charge (31.3%), type of sand (25.1%) and type of resin (9.3%). An interaction charge/type of sand was also identified (11.9%).

Figures 3 to 5 illustrate the main effects and interactions of the controlling factors.

Table 4.

Main results of the ANOVA.

|  |  | Max. Load |  | Flexural Strength |  | Flexural Toughness |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Factors: | DF | P-Value | % Contrib.(P) | P-Value | % Contrib.(P) | P-Value | % Contrib.(P) |
| Type of Resin | 1 | 0.0001 | 3.58 | 0.0001 | 3.56 | 0.0001 | 9.31 |
| % of Charge | 1 | 0.0001 | 56.82 | 0.0001 | 56.80 | 0.0001 | 31.29 |
| % Resin | 1 | 0.0589 | 0.21 | 0.0577 | 0.22 | 0.0034 | 1.97 |
| Type of Sand | 1 | 0.0001 | 17.75 | 0.0001 | 17.77 | 0.0001 | 25.12 |
| Post-cure | 1 | 0.0015 | 0.84 | 0.0015 | 0.84 | 0.0208 | 1.07 |
| Type of Resin * % of Charge | 1 | 0.2762 | 0.02 | 0.2779 | 0.02 | 0.8149 | 0.21 |
| Type of Resin * % Resin | 1 | 0.0865 | 0.16 | 0.0837 | 0.17 | 0.0031 | 2.02 |
| Type of Resin * Type of Sand | 1 | 0.0001 | 2.44 | 0.0001 | 2.44 | 0.0001 | 4.91 |
| Type of Resin * Post-cure | 1 | 0.3869 | 0.02 | 0.3905 | 0.02 | 0.0296 | 0.91 |
| % of Charge * % Resin | 1 | 0.2397 | 0.03 | 0.2379 | 0.03 | 0.0226 | 1.03 |
| % of Charge * Type of Sand | 1 | 0.0001 | 9.53 | 0.0001 | 9.50 | 0.0001 | 11.91 |
| % of Charge * Post-cure | 1 | 0.0001 | 2.28 | 0.0001 | 2.28 | 0.0584 | 0.62 |
| % Resin * Type of Sand | 1 | 0.8420 | 0.07 | 0.8461 | 0.07 | 0.6800 | 0.18 |
| % Resin * Post-cure | 1 | 0.0318 | 0.31 | 0.0324 | 0.30 | 0.3377 | 0.01 |
| Type of Sand * Post-cure | 1 | 0.0001 | 2.57 | 0.0001 | 2.59 | 0.3215 | 0.00 |
| Residual | 32 |  | 3.37 |  | 3.39 |  | 9.44 |
| Total | 47 |  | 100.00 |  | 100.00 |  | 100.00 |

Figure 3. Effects of the % of charge and type of sand on maximum load.

Figure 4. Effects of the % of charge and type of sand on flexural toughness.

Figure 5. Interaction of the type of sand/% of resin on maximum load and flexural toughness.

4.  CONCLUSIONS

The analysis of the results show that:

- epoxy concrete has higher strength and flexural toughness strength and than polyester concrete;

- the % of charge (calcium carbonate) is the variable that affects the most the mechanical properties. This charge is added to resin, prior to mixing;

- The type of sand also influences significantly the mechanical properties of both epoxy and polyester concrete;

- Post-curing increases mechanical properties of both epoxy and polyester concrete. However, such influence is smaller than % of charge;

- A significant interaction was identified between the % charge and sand type as far as strength and toughness is concerned;

- The effects of type and percentage of resin are small compared with other factors leading to the conclusion that the use of cheaper resins might be cost effective.

## ACKNOWLEDGEMENTS

The support of Fundação para a Ciência e Tecnologia under project PRAXIS/C/ECM/12277/1998, “Desenvolvimento de novos betões poliméricos”, is gratefully acknowledged. The support of the European Commission under Brite/Euram contract. BRPR CT98-0708 “Highly durable precast special concrete reinforced with non-metallic rebars” is also gratefully acknowledged.

## REFERENCES

- ACI Committee 548, Guide for the use of polymers in concrete (ACI 548, IR-86), American Concrete Institute, Detroit, 1986.

- J.Dikeou, Precast polymer concrete in the United States, Proceedings of the Fifth International Congress of Polymers in Concrete, Brighton, England, 1987,
pp.251-256.

- K.S.Rebeiz and D.W.Fowler, Flexural strength of reinforced polymer concrete made with recycled plastic waste, ACI Structural Journal, 1996, pp.524-530.

- K.S.Rebeiz, S.P.Serhal, D.W.Fowler, Recommended design procedure in shear for steel-reinforced polymer concrete, ACI Structural Journal, 1993, pp.562-567.

- J.T.San José and J.L.Ramirez, FRP bars in the bending behaviour of the polymer concrete, IRF International Conference, Porto, 1999.

- J.T.San José and J.L.Ramirez, Pure bending in polymer reinforced concrete-Design guidelines for polyester polymer concrete, Proceedings of Arquimacom, 98, Bordeaux, France, 1998.

- P.P.Camanho, R.M.Guedes, A.J.M.Ferreira and A.A.Fernandes, Flexural behaviour of polymer mortar, IRF International Conference, Porto, 1999.

- G.Taguchi, System of experimental design, Unipub/ASI, 1987.

- G.Taguchi and S.Konishi, Taguchi methods, orthogonal arrays and linear graphs, American Supplier Institute, 1987.

- Figueiredo, M., Fernandes, A.A., O Método de Taguchi no planeamento e análise de operações de soldadura,Ingenium, 2ª Serie, nº11, Agosto-Setembro, 1996,
pp.79-85.

- P.Ross, Taguchi techniques for quality engineering-loss function, orthogonal experiences, parameter and tolerance design, McGraw-Hill, 1988.

Поступила в редакцию 11 октября 2000 года.