# ON THE NUMERICAL INTEGRATION OF A POROELASTOPLASTICITY MODEL. Application to the composite material

A.Salih*, O.Fassi Fehri**, S.Charif D’Ouazzane***, L.Jezequel****, Min.Ichchou****

*Industrial Engineering Laboratory, E.N.S.E.T. B.P. 6207 Rabat Instituts- Rabat - Maroc

**Laboratoire de Mécanique et Matériaux, Faculté des Sciences B.P. 1014 Rabat - Maroc

***Laboratoire de Modélisation et Calcul en Mécanique, E.N.I.M. B.P. 753 Rabat - Maroc

****Laboratoire de Tribologie et Dynamique des Systèmes, Ecole Centrale de Lyon ECULLY Cedex, France

## Abstract

An unconditionally stable algorithm for the numerical integration of poroelastoplastic constitutive relations is analysed in detail in this paper. The constitutive equations of poroelasticity are interpreted according to the micromechanical considerations. The "effective stress" formulation is also introduced. The tangent moduli resulting from this integration algorithm are obtained by consistent linearization of the poroelastoplastic constitutive equations. The algorithm is applied to Gurson's constitutive model and explicitly extended to the composite material. The tensile test simulation is solved in the ABAQUS general purpose finite element program. The finite element results are compared with those obtained from the experimental study.

## introduction

In recent years the finite element method has been successfully used to analyse structures or processes presenting non-linear, inelastic behaviour. Most inelastic constitutive models, such as rate-independent poroplasticity, define the rate of inelastic strain and the "variation of fluid content" in term of stress and pore pressure, and set of state variable. Typically, the solution to these non-linear problems is performed incrementally and numerically.

There is considerable interests for the integration of elastoplastic constitutive equations. Kierg and Kierg [1] were the first to study the accuracy of several integration algorithms for the special case of von Mises yield condition to which is associated perfect plasticity. Schreyer et al. [2] presented similar results including hardening. The stability properties of several schemes were discussed by Nagtegaal and De Jong [3]. More recently, Aravas [4] presented in details the backward Euler method for the integration of a class pressure-dependent plasticity laws. Aravas integrates the cinematic aspects of this model by using the algorithm proposed by Hunghes and Winget [5].

A detailed analysis of the backward Euler method for the integration of the poroelastoplastic constitutive equations is presented in this work. The formulation takes into account the strain and the pore pressure. It is not restricted to any particular yield condition or flow rule.

The theory of isotropic poroelasticity is introduced in section 2. The Hooke's relations and micromechanical constitutive constants are briefly listed in order to facilitate the engineering applications. A detailed description of the poroelastic theory was first given by Biot [6]. An extended review of the development of the isotropic theory can be found in Detournay and Cheng [7]. Considering the same formality of Hooke's law, the extension of the isotropic theory to an anisotropic case was achieved by Cheng [8]. Carroll [9], Thompson and Willis [10] presented micromechanical analysis. Based on the above remarks, and working with the Caussy [11] approach, the poroelastoplastic constitutive models are explicitly developed in section 3. In section 4, the backward Euler method and the "linearization moduli" resulting from this integration are presented. In section 5, a brief description of the experimental method is given. Using the dilatometry theory, the terminology used and the technique for obtaining the experimental data are based on ref.[12] for dilatometry and porosity approaches. The porous material model that has been developed by Gurson [13], and the applications of the backward Euler integration to that model are also given in section 5. The numerical study of tensile tests, using Gurson's model, are solved and compared with the experimental results in section 6.

## 2. poroelastic constitutive relations

Similar to elasticity, we define the dynamic and cinematic parameters as σij - the total stress tensor and εij - the strain tensor of the porous media. Extension to poroelasticity requires the addition of a scalar dynamic quantity p - the pore pressure, and its cinematic counterparts  - the variation of the fluid content. The physical meaning of  will be more clearly demonstrated when the micro-mechanics is presented.

The linear (or incrementally linear) stress-strain relations of a reversible deformation process can be constructed according to the formality of the generalised Hooke's law:

σij=Cijklαεkl											(1)

p=M(ζ−αεkk)										(2)

where Cijklα is the modulus tensor

Cijklα=Kα−23.Gα.δijδkl+2.Gαδikδjl							(3)

The physical meaning of these Hookean coefficients can be obtained by conducting a series of "thought experiments"; the drained (α=d) and undrained (α=u) tests.

In the drained test, the pressure p (or the perturbation of p in the incremental case) is zero. The coefficients Cijkld are identical to those of elasticity.

In the undrained test, the variation of the fluid content is zero. The undrained modulus tensor Cijklu, which characterises the apparent elastic moduli of the combined solid (matrix) and fluid constituents, satisfies the following relation:

Cijklu=Cijkld+α2M										(4)

therefore

Ku=Kd+α2MandGu=Gd							(5)

where α is the Biot's coefficient and M is a modulus associated with the combined fluid/solid compressibility [6].

α=1−KdKm		and		M=Km1−KdKm−φ01−KmKf			(6)

where Kd is the drained bulk modulus. Km and Kf are the bulk modulus of the matrix and fluid respectively.

The concept of "effective stress" played an important role in the development of soil mechanics [14]. In this context, the matrix stress (σijm) is related to the porous material stress (σij) by the "Biot effective stress" relation as:

σij=σijm−αp										(7)

In particular case, the "Terzaghi effective stress" corresponds to setting α=1. Where σijm satisfies the relation:

σijm=Cijkldεkl											(8)

The above constitutive relations were based on "bulk parameters" of total stress and strains. The micromechanical analysis reveals more physical insight. Based on this notion, the total strain tensor εij can be decomposed into a matrix, εijm, and a pore part, εij(p):

εij=(1−φ0)εijm+φ0εij(p)									(9)

The total stress tensor can be similarly decomposed as follows:

σij=(1−φ0)σijm−φ0p									(10)

A comparison with equation (7) reveals that the Biot coefficient (α) corresponds to initial porosity (φ0).

The variation of fluid content  used in the equation (2) is related to ε(p) in the following fashion:

ζ=φ0ε(p)+(φ−φ0)									(11)

where φ0 and φ are, respectively, the initial and current porosity. Using the equation (9), we can rewrite equation (11) as such:

ζ=ε−1−φ0εm+φ−φ0								(12)

## 3. poroelastoplastic constitutive relations

The class of poroelastoplastic constitutive models considered in this paper will be described in the following section.

We assume a strain and "variation of fluid content" rates decompositions in the following equations:

dε=dεe+dεp										(13)

dζ=dζe+dζp										(14)

where dε and d are, respectively, a differential change in the total strain and total "variation of fluid content". dεe and dεp are a differential change in the elastic and plastic strain. de and dp are a differential change in the elastic and plastic "variation of fluid content". A discussion on the definition of the strain and "variation of fluid content" measure will be raised in the section 4.

For the isotropic case, the yield function includes not only the first and the second invariants of the stress tensor but also pore pressure and state variables. This yield function is illustrated by the following formula:

Φ(σH,σq,p,Hα)=0									(15)

where σH is the hydrostatic stress

σH=13σ:I											(16)

and σq is the equivalent stress

σq=(32s:s)										(17)

Hα, α=1,2,…,n , is a set of scalar. I is the second order identity tensor and s is the stress deviator. The function Φ is defined whenever Φ<0 the response is purely poroelastic.

The flow rule is written as such:

(dεp,dφp)=dλ∂g∂σ,∂g∂p,								(18)

where dλ is a potential scalar, dφp a differential change in the plastic porosity and g=g(σH,σq,p,Hα)is the flow potential. For the rate independent materials dλ is determined by cinematic solution at each point considered. Using (16) and (17), the flow rules becomes

dεp=dλ∂g∂σqn+13∂g∂σHI								(19)

and

dφp=dλ∂g∂p,										(20)

where

n=32σqs.					 						(21)

With this notation, the rate total strain can be written as:

dεp=13dεHpI+dεqpn									(22)

The stress tensor can be written as:

σ=σHI+23σqn,										(23)

where, using the equations (7) and (23) the hydrostatic stress is also written as :

σH=σHm−αp										(24)

The poroplasticity model is achieved by describing the evolution of the state variables

dHα=hα(dεp,dφp,σ,p,Hβ)								(25)

for rate independent materials hαmust be homogenous of degree one in dεp and dφp.

## 4. Numerical integration of the poroelastoplastic constitutive relations

### 4.1. Description of the method.

Similar to the elastoplasticity, we should also use the suggestion of Aravas [4] to treat the integration of poroelastoplastic problem. This method is based on the backward Euler method.

The integration of the poroelastoplastic constitutive equations presents an interesting numerical problem. Consequently, the plastic strain and "variation of the fluid content" are defined as a rate, and the behaviour of the material changes at yield.

During the constitutive calculations in an increment, the stress, pore pressure and state variables are known at time t (beginning of the increment). The stress, pore pressure and state variables need to be updated at t+t (end of increment) when a total increment strain (Δε) and the "variation of the fluid content" () are given. This condition, as a consequent, will satisfy the yield condition and flow rules. To fulfil this, we consider the following poroelasticity equations:

σt+Δt=Cαεt+Δte=Cα(εte+Δεe)=σe−CαΔεp					(26)

pt+Δt=Mζte+Δζe−αεHte+ΔεHe=Mζte+Δζ−Δζp−αεHte+ΔεH−ΔεHp=pe−MΔζp−αΔεHp					(27)

where

σe=Cα:(εte+Δε)									(28)

and

pe=Mζte+Δζ−αεHte+ΔεH							(29)

are the poroelastic predictors. t is the time at the start of the increment, and t+t is the time at the end of the increment. In the equations (28) and (29), εte(resp.ζte) is the rotated elastic strain (resp. "variation of the fluid content") at the start of the increment.

Where, using equation (12),

Δζp=ΔεHp−1−φ0ΔεHpm+Δφp							(30)

The values of p are determined when the definition of Δφpand ΔεHpmis given.

The yield function and the flow rules are written as:

Φ(σHt+Δt,σqt+Δt,pt+Δt,Ht+Δtα)=0								(31)

and

Δεp=13ΔεHpI+Δεqpnt+Δt									(32)

where

ΔεHp=Δλ∂g∂σHt+Δt									(33)

Δεqp=Δλ∂g∂σqt+Δt									(34)

and

Δφp=Δλ∂g∂pt+Δt										(35)

The elimination of Δλ, in the equations (33), (34) and (35), gives

ΔεHp∂g∂σqt+Δt−Δεqp∂g∂σHt+Δt=0							(36)

and

ΔεHp∂g∂pt+Δt−Δφp∂g∂σHt+Δt=0							(37)

Using the equation (24), we can rewrite (23) as:

σt+Δt=(σHmt+Δt−αpt+Δt)I+23σqt+Δtnt+Δt						(38)

Figure1 shows the geometric interpretation of the algorithm in (σ, p) space. Using the equations (3) and (32), we can rewrite the equations (26) and (27) as:

σt+Δt=σe−KαΔεHpI−2GαΔεqpnt+Δt							(39)

pt+Δt=pe−MΔζp−αΔεHp								(40)

and the evolution of the state variables is given through:

ΔHα=hα(Δεp,Δφp,σt+Δt,pt+Δt,Ht+Δtβ)						(41)

t , pt)

e,p e)

Figure 1: Geometric interpretation of the backward Euler algorithm in (, p) space.

The above equations show that, in deviatoric stress space, the yield surface is along nt+Δt which means that se and st+Δt are co-axial. Therefore nt+Δt can be simply determined by the elastic predictor σe as:

nt+Δt=32σqese

This implies the following consequences:

- the flow rule is independent to the third invariant of the stress tensor,

- linear isotropic poroelasticity makes C: nt+Δt co-axial with nt+Δt.

The above observations reduce the number of unknowns. In general, for a 3-dimensionnal problem, we need to solve for all the seven independent components: six stresses and one pore pressure at t+Δt. As result, the equation (38) shows that, when nt+Δt is known, the scalars σHt+Δtandσqt+Δt define completely the stress tensor at the end of the increment. Similarly, the equation (32) shows that Δεp is determined in terms of the two scalars: ΔεHp and  Δεqp.

Using the poroelasticity equations (38) and (39), we find

σH=σHm−αp=σHe−KαΔεHp								(42)

σq=σqe−3GαΔεqp 									(43)

Δεqpand ΔεHp are related by the "dilatancy " relation [11]

∂ΔεHp∂Δεqp=δn											(44)

where δ is the dilatational factor.

The equation (41) can be written as

ΔHα=hα(13ΔεHpI+Δεqpn,Δφp,(σHm−αp)I+23σqn,Hβ)			(45)

As a Summary, the previous poroelastoplastic integration problem is reduced to the following non-linear equations:

ΔεHp∂g∂σqt+Δt−Δεqp∂g∂σHt+Δt=0							(46)

ΔεHp∂g∂pt+Δt−Δφp∂g∂σHt+Δt=0							(47)

Φ(σH,σq,p,Hα)=0									(48)

σH=σHe−KαΔεHp										(49)

σq=σqe−3GαΔεqp										(50)

p=pe−MΔζp−αΔεHp								(51)

Δζp=ΔεHp−1−φ0εHpm+Δφp								(52)

ΔHα=hα(ΔεHp,Δεqp,Δφp,σH,σq,p,Hβ)						(53)

for ΔεHp,Δεqp,Δφp,σH,σq,p and   ΔHα, α=1, 2, ..., n.

These equations are solved using Newton's method. We chooseΔεHp,  Δεqp and  Δφp as the primary unknowns, treating the equations (46), (47) and (48) being the basic equations in which σH,σq and  ΔHαare defined by the equations (49), (50) and (53). cH , cq and c which are the corrections for ΔεHp,  Δεqp and  Δφpare obtained by the following Newton equations:

A11cH+A12cq+A13cφ=b1A21cH+A22cq+A23cφ=b2A31cH+A32cq+A33cφ=b3								(54)

where the constants Aij and bi are given in the Appendix I.

When cH, cq and c are defined the values of ΔεHp,  Δεqp and  Δφpare updated according to :

ΔεHp→ΔεHp+cHΔεqp→Δεqp+cqΔφp→Δφp+cφ										(55)

The values of σH, σq and pare updated using the equations (49), (50) and (51). Finally, the increments of the state variables are updated by solving the equations included in (53). This iteration is continued till ΔεHp,  Δεqp and  Δφp converge.

The derivation of the equations, which are developed in the appendix I, are completely defined with the yield function, the flow potential and state variables.

When the Δφp is defined as state variable, the Newton equations are, greatly, reduced.

### 4.2. Linearization moduli.

The problem of the implicit finite element method is solved by the discretization of the non-linear equations for the each nodal. If a full Newton scheme is used to solve these non-linear poroelastoplastic equations, one needs to calculate the so-called "linearization moduli".

D=∂σ∂εt+Δt										(56)

The moduli D defines the variation in stress at t+t that is caused by a variation of the total strain at t+t. D depends on the algorithm used for the integration of poroelastoplastic constitutive equations

σ=Cα:ε−εtp−13ΔεHpI−Δεqpn							(57)

where

∂σ=∂ε−13∂ΔεHpI−∂Δεqpn−Δεqp∂n∂σ:∂σ					(58)

where, using the equation (21),

∂n∂σ=1σq32J−12II−nn								(59)

where

Jijkl=δik.δjl

is the fourth order identity tensor with Cartesian components.

In the following we calculate the variations ∂ΔεHp,  ∂Δεqp.

Using equations (36) we find

∂ΔεHp∂g∂σq+ΔεHp∂2g∂σH∂σq∂σH∂σ+∂2g∂σq2∂σq∂σ:∂σ+α=1n∂2g∂σq∂Hα∂Hα−∂Δεqp∂g∂σH−Δεqp∂2g∂σH2∂σH∂σ+∂2g∂σH∂σq∂σq∂σ:∂σ+α=1n∂2g∂σH∂Hα∂Hα=0	(60)

The yield condition (equation (15)) also gives

∂Φ∂σH∂σH∂σ+∂Φ∂σq∂σq∂σ:∂σ+α=1n∂Φ∂Hα∂Hα=0 					(61)

Using the equation (25) we find

∂Hα=β=1n∂Hα∂hβ∂hβ∂ΔεHp∂ΔεHp+∂hβ∂Δεqp∂Δεqp+∂hβ∂σH∂σH∂σ+∂hβ∂σq∂σq∂σ:∂σ	(62)

Taking into account that:

∂σH∂σ=13Iand∂σq∂σ=n								(63)

the equations (60) and (61) can be rewritten as:

A11∂ΔεHp+A12∂Δεqp=B11I+B12n:∂σ						(64)

A21∂ΔεHp+A22∂Δεqp=B21I+B22n:∂σ						(65)

where the constants Aij and Bij are given in Appendix II. The equations (64) and (65) are solved in order to give ∂ΔεHp and  ∂Δεqp. So:

∂ΔεHp=mHII+mHnn:∂σ								(66)

and

∂Δεqp=mqII+mqnn:∂σ								(67)

The substitution of ∂ΔεHp and  ∂Δεqpinto (58) allows to find that:

J+Cα:T:∂σ=Cα:∂ε								(68)

where

T=13tHIII+13tHIIn+tqInI+tqnnn+Δεqp∂n∂σ						(69)

Finally, by the means of the equation (68), the moduli is found to be

D=∂σ∂εt+Δt=J+Cα:T−1:Cα							(70)

which can be written as :

D=T+Cα−1−1										(71)

D is symmetric if

13tHn=tqI

The quantities tHn  and  tqI represent the coupling between the deviatoric and hydrostatic behaviour of the material.

## 5. APPLICATION

### 5.1. Experimental.

The mechanical behaviour of multiphase materials is closely related to the interfacial adhesion between the various components. There is a considerable interest in the development of experimental techniques for the characterisation of interfacial debonding. Probably, the best known technique is tensile dilatometry which is recently reviewed by Naqui and Robinson [15].

###### Material

The material used in this study is constituted by the Glass Beads (type E) incorporated in the Polyester (UP) resin. The average beads diameter is about 350µ.

During the moulding of these constituents, the pores remain in the composite, because of resin viscosity. The beads volume fraction fN and the initial porosity 0 are obtained by the statistical method which is described in the Ref. [12]. Using a microscope (Versamet-2), which magnified 1600X, the material is visualised. See figure 2.

The initial porosity 0 is easily proved by the following equation:

φ0=1−fNf0											(72)

where f0 is the beads volume fraction corresponding at 0 =0. Experimentally, in most cases, the value of f0 can be estimated to 0.52.

Figure 2: Microscopic section of sample (beads in white, pores in black, resin in clear)

(                - 0.1 mm).

###### Technical test

In the case of the undrained test, in which the "variation of the fluid content" is zero, the technique used for determining the experimental data is the tensile test.

A tensile test machine with the cross-head speed at 1mm/mn was used. The strain data is collected by using two extensometers: axial extensometer and transverse extensometer (gag length 10mm). The strains () and the stresses () were, simultaneously, recorded.

The stress  versus strain  curves, for various initial porosity (0), are shown in figure 3. The values of the pore pressure are presented in figure 4. The pore pressure is determined by the "effective stress" relation in which the Biot's coefficient is calculated by the equation (6).

Figures 3 and 4 show that the stress decreases with the porosity content but the pore pressure increases with the porosity content. The behaviour of these materials is nonlinear. The most plausible reason on this nonlinearity is the debonding process. The effect of treatment of the glass beads interface appears negligible. It is difficult to separate the contribution of debonding and the behaviour of the matrix because almost all the glass beads have became debonded from the matrix. From this study, the interfacial debonding is characterized by the current porosity ().

###### Porosity model

The model adopted for these porous materials is defined by periodic array of spherical pores in an elastic-plastic medium. Referring to the microscopic scale, we also denote that R0 is the initial pore radius and dΩ0m=A03 is the elementary volume of the matrix. See figure 5.

2R0

A0

Period Y

Figure 5: Periodic array of spherical pores.

The change in pore volume fraction during an increment of deformation is partly due to the growth of the existing pores and partly due to the nucleation of the new pores by cracking or interfacial decohesion of inclusions. Accordingly we write:

dφ=dφG+dφN										(73)

The matrix is assumed to satisfy the elastic-plastic behaviour. However, the macroscopic response does not because of the existent pores. The growth porosity is related to the change of the total volume as:

dφG=(1−φ0)dεHp										(74)

From the experimental study, we consider the cumulated strain (q) that controls the nucleation of the pores [16]

εq=2.lnRcR0=23lnRcA0A0R03                        =23lnφNφ0								(75)

where

φN=43πRc3A03andφ0=43πR03A03							(76)

R0 and Rc are, respectively, the initial and critical pore radius.

Using the equations (44) and (75), the rate of the nucleation porosity dN is obtained by the following formula:

dφN=32φ0δexp32εHpδdεHp=SdεHp							(77)

where  is the dilatational factor.

Figure 6 shows that the porosity, which is changing, is determined as it undergoes mechanical behaviour. In tension test, the porous material is soften by the growth and the nucleation of the pores.

### 5.2. Gurson's model

In this section, the material model, which is developed by Gurson [13] on a ductile material containing a spherical pores, will be applied on the material studied. Based on a rigid-plastic matrix which contains spherical pores, Gurson proposed the yield condition of the following form:

Φ=σqσ02+2.q1φcosh32q2σHσ0−1+q3φ2=0					(78)

where 0 is the equivalent stress representing the actual microscopic stress state in the matrix material, and  is the current porosity. The parameters q1 , q2 and q3=q12 were introduced by Tvergaard [17] in an attempt to make the predictions of Gurson's equations. This assumption agree with numerical studies of materials containing a pores periodically distributed in the matrix. The yield surface given by the equation (78) becomes that of von-Mises (which is assumed in Gurson's model to hold the matrix material) when =0. Whenever the pore volume fraction is non-zero, there is an effect of the hydrostatic stress on the plastic flow. This is illustrated in figure 7.

It should be noted that =0 implies that the material is fully dense, and the Gurson yield condition is reduced to that of von Mises. =1 implies that the material is fully voided and has no stress carrying capacity. Figure 7 compares the behaviours of porous metal, which has an initial porosity 0.

Using the equations developed in the precedent section, the flow rules are defined as:

dεp=dλ13∂Φ∂σHI+∂Φ∂σqn								(79)

In Gurson's model, the microscopic equivalent plastic strain (εp) is assumed to be governed by the equivalent plastic work:

σdεp=(1−φ)σ0dεp									(80)

or		dεp=σdεp(1−φ)σ0									(81)

Similar to the equation (73), the evolution of the porosity is defined as:

dφ=dφG+dφN

where

dφG=(1−φ0)dεp:IanddφN=Ad {εp						(82)

Chu and Needleman [18] suggested that the parameter A is defined in the following :

A=fNsN2πexp−12εp−εNsN2						(83)

where fN is the volume fraction of pore nucleating particles, N is the normal distribution of the nucleation strain, and sN is the standard deviation.

Using the notation of section 4, the necessary equations for the application of the backward Euler method can be summarised in:

Φ=g=σqσ02+2q1φcosh32q2σHσ0−1+q3φ2=0			(84)

σ=σH−αpI+23σqn								(85)

p=−αMΔεHp										(86)

Δεp=13ΔεHpI+ΔεHpn								(87)

ΔH1=Δεp=σHΔεHp+σqΔεHp1−φ0σ0							(88)

ΔH2≡Δφ=AΔεp+1−φ0Δεp							(89)

## 6. numerical implementation

The Backward Euler integration, described in the previous sections, was implemented in the ABAQUS general purpose finite element program [19]. This code provides a general interface so that the user may introduce his own constitutive model in a "user subroutine". In ABAQUS, the cinematic aspects of the model are first integrated by using the algorithm proposed by Hunghes and Winget [5].

In the following, we will numerically simulate the uni-axial tension test by using the Gurson's model to describe the constitutive behaviour of the material. The studied test is the uni-axial tensile applied on the element including the 20-node bricks. The element and the boundary conditions are shown in figure 8. The displacement test is controlled by the equal increments of 2.5 percent in the original length.

Figure 8: Uni-axial tensile test.

Z

x

y

2

3

10

15

19

7

14

6

8

16

5

13

18

17

20

11

4

12

1

9

The results of the finite element analysis are then compared with those that are experimentally obtained. From this comparison, let us consider the behaviour of the composite material with an initial porosity at 0=0.2.

The matrix material study is the UP resin. In the range of axial strain which is studied, the behaviour of the neat UP is linear. Where the modulus Em=4000 MPa and the Poisson ratio =0.4. The equivalent plastic strain (εp) representing the microscopic strain-state in the material, is assumed to be related to the stress  through a following relation:

εp=σ−σ0Emδ1−φ0N									(90)

where Em is the matrix Young modulus and N is the hardening exponent (N=1.3),  is the dilatational factor (=0.17). The initial porosity is about 0=0.2 and the Tvergaard constants are equal to q1=q2=q3=1.

The plastic strain which controls the nucleation process is described by the volume fraction of pore nucleating particles fN=0.04. The nominal strain for nucleation N=0.03 and the standard deviation sN=0.1.

In the range of axial strain which is studied (0-0.6%), the curve of stress , pore pressure p, and current porosity , are respectively plotted in figures 9, 10 and 11. Those figures show that, the finite element results agree very well with the experimental results.

## 7. conclusion

In this work, we have applied the backward Euler method on the integration of the poroelastoplastic constitutive equations. The yield function and flow potential, which depend on the hydrostatic and Mises stress, has been analysed in details. The formulation is not restricted to any particular yield condition, flow rule, strains, porosity or rotations of finite size.

The backward Euler method is particularly suited for general purpose finite element programs. It is unconditionally stable and it is also the most accurate member of the generalised trapezoidal integration.

The strain and the porosity increments are obtained by the Newton’s integration method. This method was mentioned in Ref. [4]. Under certain circumstances, the use of alternative solution schemes such as quasi-Newton or secant-Newton methods may become preferable.

The linearization moduli resulting from the backward Euler method can be easily calculated. In general, the derivation of the Jacobean by Newton’s method, is complicated. In some cases, it can only be numerically defined.

The poroelastic formulation is developed, in the isotropic cases, according to the micromechanical considerations. The application of the backward Euler integration algorithm on the Gurson’s model is discussed. The Gurson’s material is extended to the porous composite material, and the tensile test simulation is solved in the ABAQUS general purpose finite element program.

In the experimental study, we have applied the Bridgman [20] approach in calculating the current porosity. The pore pressure is obtained by the "effective stress" approach. This study was encouraged by a comparison between finite element results and those experimentally obtained.

As examined here, plastic dilatation requires the presence of porosity, and when this is not initially the case, porosity can sometimes be nucleated during straining in the second phase. Nucleation in the second phase is examined in Ref. [13].

## APPENDIX I

The constants involved in the solution of the poroelastoplastic equations are written as

A11=∂g∂σq+ΔεHp−Kα∂2g∂σH∂σq+α=1n∂2g∂σq∂Hα∂Hα∂ΔεHp        −1δn∂g∂σH−Δεqp−Kα∂2g∂σH2+α=1n∂2g∂σH∂Hα∂Hα∂ΔεHp

A12=δn∂g∂σq+ΔεHp−3Gα∂2g∂σq2+α=1n∂2g∂σq∂Hα∂Hα∂Δεqp        −∂g∂σH−Δεqp−3Gα∂2g∂σH∂σq+α=1n∂2g∂σH∂Hα∂Hα∂Δεqp

A13=∂ΔεHp∂Δφp∂g∂σq+ΔεHp∂p∂Δφp∂2g∂σq∂p+α=1n∂2g∂σq∂Hα∂Hα∂Δφp        −∂Δεqp∂Δφp∂g∂σH−Δεqp∂p∂Δφp∂2g∂σH∂p+α=1n∂2g∂σH∂Hα∂Hα∂Δφp

A21=−Kα∂Φ∂σH+α=1n∂Φ∂Hα∂Hα∂ΔεHp

A22=−3Gα∂Φ∂σq+α=1n∂Φ∂Hα∂Hα∂Δεqp

A23=∂Φ∂σH∂σH∂Δφp+α=1n∂Φ∂Hα∂Hα∂Δφp

A31=∂g∂p+ΔεHp−Kα∂2g∂σH∂p+α=1n∂2g∂p∂Hα∂Hα∂ΔεHp        −∂Δφp∂ΔεHp∂g∂σH−Δφp−Kα∂2g∂σH2+α=1n∂2g∂σH∂Hα∂Hα∂ΔεHp

A32=δ.n.∂g∂p+ΔεHp−3Gα∂2g∂p∂σq+α=1n∂2g∂p∂Hα∂Hα∂Δεqp        −∂Δφp∂Δεqp∂g∂σH−Δφp−3Gα∂2g∂σH∂σq+α=1n∂2g∂σH∂Hα∂Hα∂Δεqp

A33=∂ΔεHp∂Δφp∂g∂p+ΔεHp∂p∂Δφp∂2g∂p2+α=1n∂2g∂p∂Hα∂Hα∂Δφp        −∂g∂σH−Δφp∂p∂Δφp∂2g∂σH∂p+α=1n∂2g∂σH∂Hα∂Hα∂Δφp

b1=−ΔεHp∂g∂σq+Δεqp∂g∂σHb2=−Φb3=−ΔεHp∂g∂p+Δφp∂g∂σH

where

∂Hα∂ΔεHp=β=1m∂Hα∂hβ∂hβ∂ΔεHp−Kα∂hβ∂σH

∂Hα∂Δεqp=β=1m∂Hα∂hβ∂hβ∂Δεqp−3Gα∂hβ∂σq

∂Hα∂Δφp=β=1m∂Hα∂hβ∂hβ∂Δφp+∂p∂Δφp∂hβ∂p

## APPENDIX II

The constants involved in the calculation of the moduli D are written as

A11=∂g∂σq+α=1nβ=1mΔεHp∂2g∂σq∂Hα−Δεqp∂2g∂σq∂Hα∂Hα∂hβ∂hβ∂ΔεHp

A12=−∂g∂σH+α=1nβ=1mΔεHp∂2g∂σq∂Hα−Δεqp∂2g∂σH∂Hα∂Hα∂hβ∂hβ∂Δεqp

A21=α=1nβ=1m∂Φ∂Hα∂Hα∂hβ∂hβ∂ΔεHp

A22=α=1nβ=1m∂Φ∂Hα∂Hα∂hβ∂hβ∂Δεqp

B11=−13ΔεHp∂2g∂σH∂σq+α=1nβ=1m∂2g∂σq∂Hα∂Hα∂hβ∂hβ∂σH−13Δεqp∂2g∂σH2+α=1nβ=1m∂2g∂σH∂Hα∂Hα∂hβ∂hβ∂σH

B12=−ΔεHp∂2g∂σq2+α=1nβ=1m∂2g∂σq∂Hα∂Hα∂hβ∂hβ∂σq+Δεqp∂2g∂σH∂σq+α=1nβ=1m∂2g∂σH∂Hα∂Hα∂hβ∂hβ∂σq

B21=−13∂Φ∂σH+α=1nβ=1m∂Φ∂Hα∂Hα∂hβ∂hβ∂σH

B22=−∂Φ∂σq+α=1nβ=1m∂Φ∂Hα∂Hα∂hβ∂hβ∂σq

## REFERENCES

1.	Krieg R.D. and Krieg D.B., Accuracies of numerical solutions for elastic-perfectly plastic, J. Pressure Tech., 1977, 99, pp.2-15

2.	Schreyer H.L., Kulak R.F. and Kramer M.M, Accurate numerical solutions for elastic plastic models, J. Pressure Vessel Tech., 1979, 101, pp.226-234.

3.	Nagtegaal J.C. and De Jong J.E., Some computation aspects of elastic- plastic large strain analysis, Int.J.Numer. Methods Eng., 1981, 17, pp.15-41.

- Aravas N., On the numerical integration of class of pressure-dependent plasticity models, Int.J. Numer. Methods Eng., 1987, 24, pp.1395-1416.

- Hughes T.J.R. and Winget J., Finite rotation effects in numerical integration of rate constitutive equations arising in large deformation analysis, Int. J. Numer. Methods Eng., 1980, 15, pp.1862-1867.

- Biot M.A., General theory of three-dimensional consolidation, J. Appl. Phys., 1941, 12, pp.155-164.

- Detournay E. and Cheng A.H.D., Fundamentals of poroelasticity, In Comprehensive Rock Engineering : Principles, Practice and Projects, 2, Analysis and Design Method, Edited by Fairhurst C, Pergamon Press, 1993, pp.113-171.

- Cheng A.H.D., Material coefficients of anisotropic poroelasticity, Int. J. Rock. Mech. Min. Sci., 1997, 34, pp.199-205.

- Carroll M.M., Mechanical response of fluid-saturated porous materials, In Theoretical and applied mechanics, 15th Int. Cong. Theoretical and appl. mech. Toronto, Edited by Rimrott F.J.P. and Tabarrok B., 1980, pp.251-262.

- Thompson M. and Willis J.R., A reformulation of the equations of anisotropic poroelasticity, J. Appl. Mech. ASME, 1991, 58, pp.612-616.

- Caussy O., Mécanique des milieux poreux, Edited by Editions Technip-Paris, 1991, pp.89-217.

- AFNOR Plastiques renforcés au verre textile, In France Association of Normalisation, Edited by AFNOR, 2th ed., 1982, pp.338-351 and pp.396-399.

- Gurson A.L. Continuum theory of ductile rupture by void nucleation and growth: Part I - Yiel criteria and flow rules for porous ductile materials., J. Eng. Matl. Tech., 1977, 99, pp.2-15.

- Carroll M.M., An effective stress law for anisotropic elastic deformation, J. Geophys. Res., 1979, 84, pp.7510-7512.

- Naqui S.I. and Robinson I.M., J. Matl.Sci., 1993, 28, pp.1421.

- Leblond J.-B., Perrin G. and Devaux J. An improved Gurson-type model for hardenable ductile materials, Eur. J. Mech., A/solids, 1995, 14, pp.499-527.

- Tvergaard V., Influence of voids on shear band instabilities under plane strain conditions, Int. J. Fract., 1981, 17, pp.389-407.

- Chu C.C. and Needleman A., Void nucleation effects in biaxially stretched sheets, J. Eng. Matl. Tech., 1980, 102, pp.249-256.

- Hibbitt H.D., ABAQUS/EPGEN-a general purpose finite element code with emphasis on non linear applications, Nucl. Eng. Des., 1984, 77, pp.271-297.

- Bridgman P.W., Studies in large plastic flow and fracture, Hawaed University Cambridge Messachussets, 1964.

Поступила в редакцию 26 сентября 2000 года.