New approach to establish Similitude Invariant
for Vibration Experiment
of Symmetrically Laminated Plates

Variddhi Ungbhakorn, Pairod Singhatanadgid

# Chulalongkorn University, Bangkok, Thailand

#### ABSTRACT

Similitude theory is a powerful tool to establish the sufficient and necessary conditions of similarity between the model and prototype. Recently there were several published papers on laminated plates and shells to develop the similarity conditions for the buckling and vibration problems. However, those authors have applied the similitude transformation to the solutions of the governing differential equations instead of to the governing differential equations directly. This causes serious limitation on the applicability of the similitude theory because exact or approximate analytical solutions must be obtained before they could apply the similitude transformation. This research paper is to derive the similitude invariants, hence the scaling laws, for free vibration response of symmetric cross-ply and angle-ply laminated plates by applying the similitude transformation to the governing differential equations directly. Due to scarce test data, the fundamental frequencies of vibration obtained by this approach is theoretically verified by using data of the models from theory and make substitution into the scaling laws to predict the fundamental frequencies of the prototypes and compare to the theoretical values of the prototypes. For complete similitude cases with several aspect ratios show exact agreement between results predicting from the scaling laws and from theory. But in reality, either due to the complexity of the scaling laws, or to minimize the costly experiment, partial similitude may be required. Therefore, approximate scaling laws are investigated and recommended by considering distortion in material properties, stacking sequences and number of plies.

### Nomenclature

a	plate length

Aij	laminate extensional stiffnesses

b	plate width

Bij	laminate coupling stiffnesses

C	scaling factor matrix

Ci	similitude scaling factors

Dij	laminate flexural stiffnesses

Eij	Young’s moduli of elasticity

h	total  laminate thickness

k	non-dimensional natural frequencies of free vibration

L(…) 	differential or algebraic operator

number of half waves

m	model

p 	prototype

u, v, w	middle surface displacements

	mass density

	natural frequencies of free vibration

x,y	rectangular coordinates

Xm	vector of model variables

Xp	vector of prototype variables

#### INTRODUCTION

Laminate composites are widely used for components in mechanical and aerospace engineering applications due to their high specific stiffness (stiffness per unit density) and high specific strength (strength per unit density). Any new design base on these materials usually requires extensive experiment evaluation before going to production. This arises the need for experimental verification of the approximate analytical or numerical solutions and the need for determining the relationships among system parameters by measurement before producing the prototype. Tuttle et al. [1] performed intensive experiments on the laminated plates subjected to biaxial loading using four stacking sequences and three aspect ratios. Unlike isotropic plates, they found rather large discrepancies in buckling loads between measurement and theoretical prediction, in some case up to 35%. Therefore, in general, when designing any new composite structure, the experiments performed on the prototype may be necessary. If without any other alternative, time consuming and cost in doing experiments are unavoidable. This is where the similitude method appears as an indispensable tool in order to be able to design efficient experiments to save time and cost. Similitude theory can be roughly stated to be a branch of science concerned with sufficient and necessary conditions of similarity among phenomena. If such similarity conditions can be found among parameters of the model and prototype, then the scaled replica can be built to duplicate the behaviors of the full-scaled system and the results from the model experiments can be employed to predict the behavior of the prototype which has complete similitude with the test model. As will be seen later that the statement of similitude theory is founded on a rigorous mathematical basis.

Simitses, et al. 2-5 have published several papers on buckling of cross-ply laminated plates that deal with the establishment of the similarity conditions between the two phenomena, the model and the prototype. Then they use these similarity conditions or “scaling laws” to design scaled-down models and employ the model data from theoretical calculation to predict the behavior of the prototypes from the scaling laws. They also published papers on the similarity conditions of free vibration responses for such structures [6-7]. However, they have applied the similitude theory to the solutions of the governing differential equations instead of to the governing differential equations directly. This procedure puts serious limitation on the applicability of the concept of similitude theory because some forms of exact or approximate analytical solutions must be obtained before they can apply the similitude transformation. The main objective of this study is to derive the similitude invariants for free vibration responses of the cross-ply and angle-ply laminated plates by applying the similitude transformation to the governing differential equations directly. The derived frequency invariants yield the scaling laws among the models and prototypes appropriate in design experiments. To demonstrate the validity of the scaling laws and in absence of the model test data, the authors have theoretically calculated the fundamental frequencies of the model and prototype from the available solutions, then substitute the theoretical results of the model into the scaling laws to predict the fundamental frequencies of the prototype. Besides complete similitude results, the possibility of using distorted models is also investigated.

# 2. CONDITIONS FOR COMPLETE SIMILITUDE

Considering all variables, geometric and physical, of the prototype and the model denoted by Xpi and Xmi respectively, where i = 1,2,…n. The two systems or phenomena are similar if their corresponding characteristics are connected by bi-unique (one-to-one) mappings such that

Xp = CXm

and 		Xm = C-1 Xp

Hence, the following theorem can be stated 8: The sufficient and necessary condition of similitude between two systems is that the mathematical model of the one be related by a bi-unique transformation to that of the other.

Mathematical models of similar systems are invariable under similitude transformation. Hence, the differential equations of any two similar systems must coincide, i.e.

L(Xmi) = L(Xpi)										(1)

Let the model and prototype variables be related to each other by the equations:

Xpi  = CiXmi											(2)

Substitute eq. (2) into (1),

L(Xmi) = L(CiXmi)

From the above theorem, it is necessary that,

L(Xmi)   =   (Ci) L(Xmi)

where (Ci) is the functional relationship among the transformation parameters. Therefore it is compulsory that

(Ci) = 1

Hence, the condition for the two systems to be similar is that the function linking the transformation parameters equals to unity. The equation (Ci) = 1, is accordingly called the similitude invariant. Now the authors shall apply the above theory to the governing differential equations for free vibration of the symmetric cross-ply and angle-ply laminated plates directly.

# 3. VIBRATION OF SYMMETRIC CROSS-PLY LAMINATED PLATES

For laminates that are symmetric in both geometry and material properties about the middle surface, the general stiffness equations will simplify considerably. The symmetric cross-ply laminates have their major principal material directions alternating at 00 and 900 to the laminate axes, for example, [0/90/90/0]. When thicknesses, locations, and material properties of the laminate are symmetric about the middle surface of the laminate, coupling between bending and extension is eliminated. In this case,

Therefore, symmetric laminates are least difficult to analyze and produce and commonly used as structural components where weight-efficient structures are needed. In derivation of the governing equations the following assumptions are fundamental to lamination theory:

1. The laminate consists of perfectly bonded laminae.

2. Each layer is a homogeneous material with known effective properties.

3. Each layer is in a state of plane stress.

4. Normals to the middle surface remain straight and normal to the deformed middle surface after deformation.

5. Normals to the middle surface are inextensional.

Consider the free vibration of the symmetric cross-ply laminated plates the governing differential equations for vibration response analysis of this case are decoupled and therefore, after dropping the variational symbol , the required equation is 9:

(3)

Let the vibration response be represented by the equation w(x,y,t) = W(x,y,)eit and making substitution into eq.(3), the following equation for vibration analysis is obtained:

(4)

Let the variables of the prototype be related to those of the model through the similitude scaling factors as follows.

By applying similitude transformation to eq.(4), the following necessary conditions for the models to behave exactly as the prototype are obtained:

(5)

Let the square of the non-dimensional frequencies be,

which yields the following similitude relation :

Let the prototype and model be related with complete geometric similarity, thus eq.(5) can be written as:

(6)

Hence, for complete similarity between the prototype and its model it is required further that :

(7)

That is, the scaling factors of all laminate flexural stiffnesses must be equal. Let the scaling factors of the flexural stiffnesses be equal to Cstiff, then eq.(6) yields the following similitude invariant of the natural frequencies of vibration for the symmetric cross-ply laminated plates :

(8)

From eq.(8), the following scaling law for predicting the natural frequencies of the prototype from the model experiment can be written as:

(9)

It is seen that all CDij in eq.(7) depend on the material properties, number of plies and stacking sequence but are independent of the ply thickness, therefore two laminated plates with different ply thicknesses, but with the same stacking sequence, for example, [0/90]s and [0n/90n]s, will satisfy the similarity conditions.

4. VIBRATION OF SYMMETRIC ANGLE-PLY LAMINATED PLATES

In contrast to symmetric cross-ply laminates the symmetric angle-ply laminates are characterized by a full matrix of extensional stiffnesses as well as bending stiffnesses but still have no coupling between bending and extension, i.e. Bij = 0. Hence, the principal difference of the governing differential equation of these laminates and the symmetric cross-ply laminates is the introduction of the twisting coupling stiffnesses, D16 and D26. Therefore the differential equation governing vibration response is [9]:

(10)

Let the free vibration response of the plates be w(x,y,t) = W(x,y,)eit, then eq.(10) becomes :

(11)

The present of D16 and D26 in the free vibration differential equation makes an exact closed-form solution impossible and an approximate solution such as Rayleigh-Ritz or Galerkin procedure must be sought or numerical methods such as finite element or boundary element must be used. Apply the similitude transformation to eq.(11), with the consideration of complete geometric similarity, the following conditional equations for similarity among the prototypes and models are derived:

(12)

For complete similarity between the prototype and its model it is further required that

(13)

Hence, the scaling factors of all laminate flexural stiffnesses must be equal. Let the scaling factors of the flexural stiffnesses be equal to Cstiff, then the above equations yield the following natural frequency invariant for the symmetric angle-ply laminated plates :

(14)

which gives the following scaling law:

(15)

5. THEORETICAL SOLUTIONS FOR FREQUENCIES OF VIBRATION

In absence of the test data, therefore, for the purpose of verifying the derived scaling laws, the closed-form solution of the natural frequencies for free vibration response for each case is needed. For the case of symmetric cross-ply laminated plates, the simply-supported boundary conditions are :

Along x=0, a :

Along y=0, b :

By observing that along x=0, a, w,y =w,yy=0, and along y=0, b, w,x=w,xx=0, then the deflection function

(16)

satisfies the boundary conditions. Substituting eq.(16) into eq.(4), various frequencies, , corresponding to different mode shapes are obtained as follows.

(17)

and the fundamental frequency can be found by minimizing eq.(17) with respect to  and .

For the case of symmetric angle-ply laminated plates the simply-supported boundary conditions are:

Along x=0, a :

Along y=0, b :

By the same observation it is seen that eq.(16) satisfy all boundary conditions but not the governing differential equation (10) due to the present of D16 and D26. This renders an exact closed-form solution impossible and its solution can only be calculated from an approximate method such as Rayleigh-Ritz or Galerkin method [10]. The Rayleigh-Ritz method is used in the present study. This method begins with obtaining the total potential energy in term of displacement functions as

(18)

The out-of-plane displacement is assumed in form of a double sine series as

(19)

where  are unknown coefficients and numbers of terms used in the series are dictated by M and N. In this study the value of M and N are five, so there are 25 double sine terms used in the displacement function. The total potential energy in eq.(18) can be elaborated by performing the integrations. At this point, the only unknowns contained in the energy function are  and 2. According to the energy criterion, the total potential energy is then minimized with respect to the undetermined coefficients . This procedure yields a set of MN linear equation in the following form

where = 1, 2,…M and  = 1, 2,…N. The second term which contains summation operation vanishes if = even or = even. The system of equations can be reduced to a matrix form of generalized eigenvalue problem as

(20)

where [A] and [B] are square matrices whose elements are determined from the plate properties. [C] is a column matrix containing unknown eigenvectors, .  represents the natural frequency.

A number of eigenvalues will be obtained after the generalized eigenvalue problem shown in Eq. (20) is solved. The fundamental frequencies which are of interest in this study can be determined from the lowest eigenvalue.

6. FUNDAMENTAL FREQUENCIES PREDICTION FOR SYMMETRIC CROSS-PLY PLATES

The concept of similitude invariant applying to vibration problems of composite plates can be verified with the solutions obtained analytically. First, the fundamental frequency of model and prototype is theoretically determined. The scaling law is then applied to the theoretical solution of the model resulting in the similitude solution of the prototype. To verify the concept of similitude invariant, this similitude result is compared to the theoretical solution. For cross-ply laminates, the theoretical solution is determined according to eq.(17) and similitude solution is obtained from the scaling law in eq.(15). Both complete and partial similitude cases are presented as follows.

Complete Similitude Cases

Composite materials selected as samples in this study are graphite/epoxy, Kevlar/epoxy, and E-glass/epoxy. Their mechanical ply properties are shown in Table 1.

Table 1.

Ply properties of composites used in this study.

|  | E11 (GPa) | E22 (GPa) | G12 (GPa) | v12 | Density (g/cm3) | Ply Thickness (mm) |
| --- | --- | --- | --- | --- | --- | --- |
| Graphite/Epoxy | 132 | 10.8 | 5.65 | 0.24 | 1.54 | 0.127 |
| Kevlar/Epoxy | 76.8 | 5.50 | 2.07 | 0.34 | 1.38 | 0.127 |
| E-Glass/Epoxy | 38.6 | 8.27 | 4.14 | 0.26 | 1.80 | 0.127 |

For the results shown in Table 2, both models and prototypes have identical stacking sequence, hence their thickness and density are the same, but dimensions of the prototypes are five times larger than those of the models. Plate configurations which include materials, stacking sequences, and aspect ratios are shown in the first two columns. The 3rd and 4th columns are the fundamental frequencies of models and prototypes calculated from the theoretical solution. The last column is the frequencies of the prototypes determined from the scaling law in eq.(15) which yields exact agreement with the theoretical solution.

Table 2.

Fundamental frequencies of cross-ply laminated plates determined from theory
and similitude.

| Configuration |  | Model (b = 150 mm) | Prototype, (b = 750 mm) |  |
| --- | --- | --- | --- | --- |
| Stacking Sequence | Aspect Ratio | Theory (rad/s) | Theory (rad/s) | Similitude, p (rad/s) |
| Graphite/Epoxy [0/90]2s | 1.0 | 1357 | 54.27 | 54.27 |
|  | 1.5 | 927.0 | 37.08 | 37.08 |
|  | 2.0 | 814.8 | 32.59 | 32.59 |
| Graphite/Epoxy [90/0]2s | 1.0 | 1357 | 54.27 | 54.27 |
|  | 1.5 | 1119 | 44.78 | 44.78 |
|  | 2.0 | 1060 | 42.41 | 42.41 |
| Kevlar/Epoxy [0/90]2s | 1.0 | 1068 | 42.71 | 42.71 |
|  | 1.5 | 728.3 | 29.13 | 29.13 |
|  | 2.0 | 642.9 | 25.72 | 25.72 |
| Kevlar/Epoxy [90/0]2s | 1.0 | 1068 | 42.71 | 42.71 |
|  | 1.5 | 888.8 | 35.55 | 35.55 |
|  | 2.0 | 846.5 | 33.86 | 33.86 |

Another example of complete similitude case is shown in Table 3 where three graphite/epoxy prototypes are modeled by [0/90]2s plates.

Table 3.

Scaling law applied to laminated plates having different ply thickness and stacking sequences (Graphite/Epoxy).

| Aspect ratio | Model (rad/s) |  | Prototype (rad/s) |  |  |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | [0/90]2s |  | [02/902]2s |  |  |  |  |  | [90/0]2s |  |  |  |
|  |  |  | Theory |  | Similitude |  | % Disc. |  | Theory |  | Similitude* | % Disc. |
| 1.0 | 1357 |  | 2714 |  | 2714 |  | 0 |  | 1357 |  | 1431 | 5.49 |
| 1.5 | 927.0 |  | 1854 |  | 1854 |  | 0 |  | 1119 |  | 977.8 | -12.7 |
| 2.0 | 814.8 |  | 1630 |  | 1630 |  | 0 |  | 1060 |  | 859.5 | -18.9 |
| 2.5 | 774.3 |  | 1549 |  | 1549 |  | 0 |  | 1038 |  | 816.7 | -21.3 |
| 3.0 | 755.9 |  | 1512 |  | 1512 |  | 0 |  | 1028 |  | 797.4 | -22.4 |
| Aspect ratio |  | Model (rad/s) |  | Prototype (rad/s) |  |  |  |  |  |  |  |  |
|  |  | [0/90]2s |  | [0/90]4s |  |  |  |  |  |  |  |  |
|  |  |  |  | Theory |  | Similitude** |  | % Disc. |  |  |  |  |
| 1.0 |  | 1357 |  | 2714 |  | 2752 |  | 1.40 |  |  |  |  |
| 1.5 |  | 927.0 |  | 1957 |  | 1880 |  | -3.95 |  |  |  |  |
| 2.0 |  | 814.8 |  | 1765 |  | 1652 |  | -6.39 |  |  |  |  |
| 2.5 |  | 774.3 |  | 1696 |  | 1570 |  | -7.41 |  |  |  |  |
| 3.0 |  | 755.9 |  | 1664 |  | 1533 |  | -7.90 |  |  |  |  |

* Calculated base on

** Calculated base on

The complete similitude is achieved in the case of [02/902]2s prototype plates. Prototypes with this stacking sequence can be considered as having the same stacking sequence as the model but with twice the ply thickness. The scaling factors of all laminate flexural stiffness, CDij, of this stacking sequence equal 8 as shown in Table 4. It should be emphasized that the densities of the prototypes in this case are twice higher than the density of the model. However, this difference does not violate the similitude requirement and, hence, the fundamental frequencies calculated from theory and scaling law are exactly identical as shown in Table 3.

Table 4.

CDij of [90/0]2s, [02/902]2s and [0/90]4s plates having [0/90]2s plate as a model (graphite/epoxy).

|  | Model | Prototype |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | [0/90]2s | [02/902]2s |  | [90/0]2s |  | [0/90]4s |  |
|  | Dij (GPa-mm3) | Dij (GPa-mm3) | CDij | Dij (GPa-mm3) | CDij | Dij (GPa-mm3) | CDij |
| D11 | 8.265 | 66.12 | 8 | 4.274 | 0.5171 | 58.14 | 7.034 |
| D12 | 0.2276 | 1.821 | 8 | 0.2276 | 1.000 | 1.821 | 8.000 |
| D22 | 4.274 | 34.19 | 8 | 8.265 | 1.934 | 42.18 | 9.867 |
| D66 | 0.4938 | 3.950 | 8 | 0.4938 | 1.000 | 3.950 | 8.000 |

Partial Similitude Cases

Considering distortion in stacking sequences of [90/0]2s and [0/90]4s prototypes in Table 3, the scaling factors of all laminate flexural stiffness CDij shown in Table 4 are not equal, thus the requirement of complete similitude is not fulfilled. However, partial similitude might be investigated by using Cstiff as the average value of all CDij. It is seen that for the 16-ply prototype [0/90]4s, the agreement is very good for all aspect ratios considered herein. The discrepancies are higher for the 8-ply prototype [90/0]2s, especially for plates with larger aspect ratios. The accuracy of partial similitude model for cross-ply plates with different number of plies is presented in Figure 1 for three aspect ratios.

Another partial similitude model considering distortion in materials is shown in Table 5. This concept is very useful for modeling high-cost-material prototypes using low-cost-material models. In Table 5, fundamental frequencies of large graphite/epoxy and Kevlar/epoxy laminates are predicted from small E-glass/epoxy plates with the same stacking sequence. In this case Cstiff is approximated from the average of all four CDij. The discrepancies are all in acceptable range for experimental purpose.

Table 5.

Modeling of [0/90]2s graphite/epoxy and Kevlar/epoxy laminates (b=750mm) from
E-glass/epoxy laminates (b=150 mm).

| Aspect Ratio | Model (E-Glass/ Epoxy) | Prototype (Graphite/Epoxy) |  |  | Prototype (Kevlar/Epoxy) |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  | Theory (rad/s) | Theory (rad/s) | Similitude (rad/s) | % Disc. | Theory (rad/s) | Similitude* (rad/s) | % Disc. |
| 1.0 | 793.5 | 54.27 | 49.95 | -7.96 | 42.71 | 39.63 | -7.20 |
| 1.5 | 552.1 | 37.08 | 34.75 | -6.28 | 29.13 | 27.57 | -5.37 |
| 2.0 | 480.3 | 32.59 | 30.23 | -7.24 | 25.72 | 23.99 | -6.73 |
| 2.5 | 450.9 | 30.97 | 28.38 | -8.354 | 24.53 | 22.52 | -8.19 |
| 3.0 | 436.3 | 30.24 | 27.46 | -9.18 | 24.01 | 21.79 | -9.24 |

Calculated base on

*Calculated base on

7. FUNDAMENTAL FREQUENCIES PREDICTION FOR SYMMETRIC ANGLE-PLY PLATES

Because of the twisting coupling stiffnesses, D16 and D26, the theoretical fundamental frequencies cannot be written in an exact closed-form solution, but will be approximated according to eq.(20).

Complete Similitude Cases

Cases of complete similarity between models and prototypes of angle-ply plates are illustrated in Table 6 for two types of stacking sequences and materials. The result showed exact agreement of fundamental frequencies of the prototype determined from theory and predicted from the scaling law. Another example of complete similitude is presented in Table 7 where [452/-452]2s graphite/epoxy plates are modeled using [45]2s plates with the same material. Prototypes are two times thicker than models. It can be shown that all CDij are identical and equal to 8, thus there is no need to approximate the value of Cstiff in the scaling law. Again, fundamental frequencies of prototypes calculated from theory and scaling law yield exact agreement.

Table 6.

Fundamental frequencies of angle-ply laminated plates determined from theory and similitude.

| Plate Configuration | Aspect Ratio | Model (b = 150 mm) | Prototype, (b = 750 mm) |  |
| --- | --- | --- | --- | --- |
|  |  | Theory (rad/s) | Theory (rad/s) | Similitude (rad/s) |
| Graphite/Epoxy [45]2s | 1.0 | 1730 | 69.21 | 69.21 |
|  | 1.5 | 1213 | 48.51 | 48.51 |
|  | 2.0 | 1002 | 40.08 | 40.08 |
| Graphite/Epoxy [0/45/90/-45]s | 1.0 | 1470 | 58.81 | 58.81 |
|  | 1.5 | 957.2 | 38.29 | 38.29 |
|  | 2.0 | 791.4 | 31.66 | 31.66 |
| Kevlar/Epoxy [45]2s | 1.0 | 1389 | 55.57 | 55.57 |
|  | 1.5 | 971.7 | 38.87 | 38.87 |
|  | 2.0 | 800.2 | 32.01 | 32.01 |
| Kevlar/Epoxy [0/45/90/-45]s | 1.0 | 1166 | 46.63 | 46.63 |
|  | 1.5 | 755.2 | 30.21 | 30.21 |
|  | 2.0 | 623.5 | 24.94 | 24.94 |

Table 7.

Fundamental frequencies of [452/-452]2s laminates (b=750mm) modeled from [45]2s laminates (b=150 mm) using graphite/epoxy composite.

| Aspect Ratio | Model [45]2s | Prototype [452/-452]2s |  |
| --- | --- | --- | --- |
|  | Theory (rad/s) | Theory (rad/s) | Similitude (rad/s) |
| 1.0 | 1730 | 138.4 | 138.4 |
| 1.5 | 1213 | 97.01 | 97.01 |
| 2.0 | 1002 | 80.16 | 80.16 |
| 2.5 | 894.7 | 71.57 | 71.57 |
| 3.0 | 832.6 | 66.61 | 66.61 |

Partial Similitude Cases

Similar to the case of cross-ply laminated plates, distorted models of symmetric angle-ply plates are investigated. Table 8 shows theoretical frequencies of [45]ns specimens in the 3rd column. The values of n range from 1 to 7 or the numbers of plies of all seven samples are 4,8,12,16,20,24, and 28, respectively. All of the laminates are Kevlar/epoxy with a=300mm and b=150mm. The laminate with n=4 or the [45]4s plate is selected as the model, while other stacking sequences are for the prototypes. The 2nd column shows stiffness scaling factors of all prototypes having [45]4s as a model. It is seen that scaling factors of the six flexural stiffnesses are divided into two groups; a group of CD11, CD12, CD22, and CD66, and a group of CD16, and CD26. By using the scaling factor of the first group, i.e. CD11, as Cstiff in the scaling law, the similitude results yield very good agreement with theory, especially plates with large number of plies. Thus, the effect of the twisting coupling stiffnesses D16 and D26 died out rapidly at number of ply equal to or greater than 8.

Table 8.

Fundamental frequencies of [45]ns having [45]4s as a model.

| Value of n in [45]ns | Scaling Factor | Fundamental frequencies (rad/s) |  |  |
| --- | --- | --- | --- | --- |
|  |  | Theory | Similitude (Cstiff = CD11) | % Disc. |
| 1 | 0.015625 : 0.0625 | 380.9 | 404.3 | 6.14 |
| 2 | 0.125 : 0.25 | 800.2 | 808.5 | 1.03 |
| 3 | 0.421875 : 0.5625 | 1210 | 1213 | 0.260 |
| 4(model) | - | 1617 | - | - |
| 5 | 1.953125 : 1.5625 | 2024 | 2021 | -0.119 |
| 6 | 3.375 : 2.25 | 2430 | 2426 | -0.183 |
| 7 | 5.359375 : 3.0625 | 2836 | 2830 | -0.221 |

Note : Using Kevlar/epoxy plates with a = 300 mm and b = 150 mm.

Table 9.

CDij of [452/-452]2s graphite/epoxy plates having [45]2s Kevlar/epoxy as a model.

|  | Model, [45]2s E-Glass/Epoxy | Prototype, [452/-452]2s |  |  |  |
| --- | --- | --- | --- | --- | --- |
|  |  | Graphite/Epoxy |  | Kevlar/Epoxy |  |
|  |  | Dij (GPa-mm3) | CDij | Dij (GPa-mm3) | CDij |
| D11 | 1.496 | 29.94 | 20.01 | 16.61 | 11.10 |
| D12 | 0.7726 | 22.04 | 28.52 | 13.72 | 17.75 |
| D22 | 1.496 | 29.94 | 20.01 | 16.61 | 11.10 |
| D66 | 0.9438 | 24.17 | 25.61 | 13.85 | 14.67 |
| D66 | 0.2522 | 7.982 | 31.65 | 4.713 | 18.69 |
| D66 | 0.2522 | 7.982 | 31.65 | 4.713 | 18.69 |

The last two tables present a study of distortion in materials. Cheaper [45]2s
E-glass/epoxy plates are used to model [452/-452]s graphite/epoxy and Kevlar/epoxy prototypes. The prototypes are five times bigger than the models, and may be considered having the same stacking sequence as the model with twice the ply thickness. Again, the results in Table 10 showed very good agreement with theory by using the first group of CDij as Cstiff. Hence, the effect of twisting coupling stiffnesses D16 and D26 can be neglected in the scaling law for plates with number of plies equal to or greater than 8.

Table 10.

Modeling of [452/-452]2s graphite/epoxy and Kevlar/epoxy plates (b=750mm)
from [45]2s E-glass/epoxy plates (b=150 mm).

| Aspect Ratio | Model [45]2s E-glass/Epoxy | Prototype [452/-452]2s |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
|  |  | Graphite/Epoxy |  |  | Kevlar/Epoxy |  |  |
|  | Theory (rad/s) | Theory (rad/s) | Similitude* (rad/s) | % Disc. | Theory (rad/s) | Similitude* (rad/s) | % Disc |
| 1 | 927.4 | 138.4 | 137.6 | -0.604 | 111.1 | 110.7 | -0.377 |
| 1.5 | 656.2 | 97.01 | 97.36 | 0.352 | 77.73 | 78.34 | 0.782 |
| 2 | 550.7 | 80.16 | 81.70 | 1.91 | 64.02 | 65.74 | 2.69 |
| 2.5 | 498.4 | 71.57 | 73.93 | 3.30 | 56.99 | 59.49 | 4.40 |
| 3 | 468.7 | 66.61 | 69.53 | 4.38 | 52.91 | 55.95 | 5.75 |

* Calculated base on

### 8. CONCLUSION AND DISCUSSION

The authors have employed the similitude transformation to establish the similitude invariants and the scaling laws for free vibration response of the symmetric cross-ply and angle-ply laminated plates. For all cases of complete similitude, the predicted fundamental frequencies of the prototypes using the data of the models from theory substitute into the scaling laws have shown exact agreement with the theoretical results of the prototypes. Hence the scaling laws will allow us to design experiments to simulate the condition of real application of the prototype without having to stick to the classical boundary conditions from theory and there no need for the solutions of the complicate differential equations. This will result in cost and time savings in designing experiments of the complex unknown phenomena to predict their behaviors according to the actual condition.

In certain situation, complete similarity is difficult to fulfill for the test model, or the experiments will be too costly, then one might relax certain condition in the scaling law to enable the construction of the test model. However, employing the partial similitude or partial similarity is allowed, provided the complete set of similitude criteria to be taken into consideration is known on the basis of the mathematical model and the error caused by disregarding the criterion can be assessed beforehand. The method presented in this research paper can also be used to verify the accuracy and correctness of other numerical methods such as the finite element and boundary element analyses or certain problems whose analytical solutions are not available but only test model data.

Notice that the derived similitude invariant is independent of the boundary conditions. This is because the effects of the boundary conditions will be included in the test data of the models. Thus, predicting the behaviors of the prototypes from the scaling law will accommodate any boundary conditions, provided both the prototype and model supports are identical along the edges. The merit of the method is very beneficial to other types of structural geometry whose available solutions are not capable of predicting the test results accurately enough. For example, the effect of imperfection sensitivity of cylindrical shells subjected to axial compression, by conjecturing that this effect is the same for both the prototype and model.

REFERENCES

- Tuttle M., Singhatanadgid P., Hinds G. Buckling of Composite Panels Subjected to Biaxial Loading, Experimental Mechanics, 1999, v.39, N3.

- Simitses G.J., Rezaeepazhand J. Structural Similitude for Laminated Structures, 
J. Composites Engineering, 1993, v.3, N7-8, pp.751-765.

- Simitses G.J., Rezaeepazhand J. Structural Similitude and Scaling Laws for Buckling of Cross-Ply Laminated Plates, Proceedings of the American Society for Composites, 1994, pp.265-274.

- Rezaeepazhand J., Simitses G.J., Starnes J.H., Design of Scaled Down Models for Stability of Laminated Plates, AIAA Journal, 1995, v.33, N3, pp.515-519.

- Simitses G.J., Starnes J.H., Rezaeepazhand J. Structural Similitude and Scaling Laws for Plates and Shells: A Review, Collection of Technical Papers-AIAA/ASME/ASCE/AHS/ASC Structures, Structural Dynamics and Materials Conference 1, AIAA, 2000, pp. 393-403 0273-4508.

- Rezaeepazhand J., Simitses G.J., Starnes J.H., Used of Scaled-Down Models for Predicting Vibration Response of Laminated Plates, Composite Structures, Elsevier Science Ltd., 1995, pp. 419-426.

- Rezaeepazhand J., Simitses G.J., Starnes J.H., Design of Scaled-Down Models for Predicting Shell Vibration Response, Journal of Sound and Vibration 195, Academic Press Ltd., 1996, pp.301-311.

- Szucs, Errin , Similitude and Modelling, Elsevier Scientific Publishing Co., New York, 1980.

- Jones R.M., Mechanics of Composite Materials, Scripta Book Co., Washington, DC, 1975.

- Whitney J.M., Structural Analysis of Laminated Anisotropic Plates, Technomic Pub. Co., Lancaster, Pa., 1987.

- Поступила в редакцию 4 октября 2001 года.