Fig.3. Derived equations for the DCB specimen including fiber-bridging.

4. STRESS DISTRIBUTION BEHIND THE CRACK-TIP

The stress distribution behind the crack-tip was investigated using the Winkler foundation model, as shown in Fig.4 [1]. The same model was applied by Ozdil and Carlsson, however only a correction factor for the compliance and fracture toughness of the glass/polyester DCB specimen was derived due to elastic foundation and crack-tip rotation. The displacement function was derived from the following governing differential equation:

d4w(x)dx4+4λ4H(x)w(x)=0.								(18)

The complete solution of Eq(18). for the DCB specimen can be found in [1], using the proper boundary and matching conditions. The displacement field in the uncracked region can be expressed as:

w(x)=6PExwH3λ3aλsin(λx)sinh(λx)−A−12sin(λx)cosh(λx)+,	(19)

where