A=sinh2(λc)+sin2(λc)sinh2(λc)−sin2(λc)+2aλsinh(λc)cosh(λc)+sin(λc)cos(λc)sinh2(λc)−sin2(λc),	(20)

B=aλsinh2(λc)+sin2(λc)sinh2(λc)−sin2(λc)+sinh(λc)cosh(λc)−sin(λc)cos(λc)sinh2(λc)−sin2(λc),	(21)

λ=614HEzEx14.									(22)

Fig.4.	Elastic foundation model of the DCB specimen and stress distribution beyond the crack-tip.

Ozdil and Carlsson recommended a correction factor for the compliance and the fracture toughness based on the former Winkler foundation model:

C=8ExwaH31+1.92HaExEz14+1.22Ha2ExEz12+0.39Ha3ExEz34														(23)

the fracture toughness can be determined by the derivative of Eq.(23) using Eq.(1):

GI=12P2a2Exw2H31+1.28HaExEz14+0.41Ha2ExEz12.		(24)

A similar expression was used by Kenane and Benzeggagh [13]. It is clear based on previous computations that this is not reasonable in high modulus composite DCB specimens. The stress and strain components in the z direction beyond the crack-tip can be expressed as:

σz(x)=Ezεz(x),									(25)

εz(x)=w(x)(H2).									(26)

According to the former equations the strain energy from the stress-field behind the crack-tip can be calculated as follows:

ΔUz=12Vσz2(x)EzdV.									(27)

Since the stress component is independent from y and z, after integration of Eq.(27) respect to y and z yields:

ΔUz=12HwEz0Δaσz2(x)dx,								(28)

where a can be determined from the stress distribution, as shown in Fig.4. It was assumed that the strain energy resulted from the stress field behind the crack-tip is distributed in the area w*a. According to this the fracture energy can be calculated by dividing the strain energy by the area w*a:

ΔGI=1wΔUzΔa=H2ΔaEz0Δaσz2(x)dx.						(29)

This fracture energy should be added to the results of Eq.(16). It must be noted that a is about 2-4 mm. According to the derived analytical expressions, the compliance and the fracture toughness was evaluated by the following procedure. In the case of no fiber-bridging (until the fourth crack length) equations given in Fig.1 were used and the fracture energy in Eq.(29) was added and multiplied with the factors in Eq.(23)-(24). The fiber-bridging was considered after the fourth crack length using Eq.(15)-(16). The fracture energy from the stress distribution behind the crack-tip was calculated using Eq.(29) and added to the former Eq.(15)-(16). Again the power factors in Eq.(23)-(24) were used to corrigate the total fracture energy. It was assumed that the fiber-bridging does not cause too much difference in the stresses behind the crack-tip in the z direction.

5. FINITE ELEMENT MODEL

The finite element code COSMOS/M 2.0 was used to carry out the analysis. Two-dimensional plain strain models were constructed to obtain numerical results for the mode-I interlaminar fracture toughness. The DCB specimens were meshed with four-noded plane strain elements (PLANE2D). TRUSS2D elements were utilized to represent the bridging fibers. In fact the J-integral is applicable only for isotropic models. Since the composites are anisotropic materials the models were constructed to include the anisotropy and the applicability of the J-integral, respectively. This problem was eliminated by creating a thin (0.15 mm) isotropic layer in the mid-plane of the specimen. It was assumed that the former modification does not affect the compliance and the fracture toughness of the specimen significantly. The J-integral was determined inside the former isotropic layer as shown in Fig.5. Inside the isotropic layer the modulus Ex was used, but it was verified and experienced, that the J-integral is not sensitive to the modulus, i.e. similar values were obtained for the fracture toughness using the through-the-thickness moduli Ez.

6. SPECIMEN DIMENSIONS, MATERIAL PROPERTIES AND LOAD/DISPLACEMENT DATA

For the present analysis the following elastic properties were assumed for the carbon/epoxy composite [2]: Ex=150 GPa, Ez=11 GPa, xz=0.25, G=6 GPa and with specimen dimensions of w=20 mm, h=2 mm and initial crack length of a0=45 mm. The same properties for the carbon/PEEK composite specimens [6]: Ex=124 GPa, Ez=10 GPa, xz=0.25, G=5 GPa and specimen dimensions of w=20 mm, h=2.65 mm and a0=20 mm.