A COMPLETE REVIEW ON FRICTION MODELS OF COMPOSITE CABLES

T. Manvel Raj and N.S. Parthasarathy*

A.M.S. College of Engineering, Muthapudupet, Chennai – 600055, Tamilnadu, India

*AU-FRG Institute for CAD/CAM, Anna University, Chennai – 600025, Tamilnadu, India

## ABSTRACT

## This paper presents a detailed review of all the existing mathematical models irrespective of their field of application to accommodate the more complex situations like friction and damping effects in multi-layered stranded cables under different load conditions like tension, torsion and bending. The various existing models for predicting the mechanical behavior of helical wire strands; cables, ACSR conductors, etc. have been critically evaluated, together with the corresponding experimental data when available. Particularly, this work is meant for the future researches in stranded cables. This review contains 291 references.

## 1. INTRODUCTION

A stranded cable is a complex structure made up of layers of wires wrapped helically around a straight central core wire (Fig.1). A property common to structural elements such as stranded cable is their ability to resists relatively large axial loads in comparison to bending and torsional loads. Because of this property is one of the oldest tools that human have used in their efforts to produce a better life for themselves. A copper cable found in the ruins of Nineveh near Babylon indicates that wire rope was used as a structural element in about 700 B.C. Stranded cable assemblies find wide spread applications in structural cables, mechanical power transmission ropes, elevators, mine hoists, cranes, conveyors, hauling devices, suspension bridges, overhead transmission line conductors, filament yarns, marine and mooring cables such as tension legs and tether for deep water platform, buoyant structures, etc. These cables are subjected to different kinds of loads in addition to different terrain conditions. The process by which a physical system is simplified to obtain a mathematically tractable situation is called modeling. The resulting simplified version of the real system is called the mathematical model, or simply the model of the system.

Fig.1. Construction of a typical multilayered stranded composite cable.

A review of such mechanical models of wire ropes with general mechanical nature was published by Costello (1978), with 30 references. The only general reference for overhead electrical power transmission conductors is EPRI’S transmission line reference book based on EPRI Research project 792, Prepared by Gilbert et al (1979). This reference book presents a state-of-the-art study of conductor fatigue, Aeolian vibration, conductor gallop, and wake-induced oscillation. Each chapter presents a detailed examination of the causes, mechanisms, incidence, types of motion, factors influencing motion, resulting damage, and protection methods associated with its particular topic.

Another review in wire ropes of general mechanical interest was published by Utting and Jones (1984) with 77 references. This has been updated by Utting (1994a, 1994b, 1995), with 110 new references. A review of mechanical models of helical strands was published in applied mechanics reviews 8 years ago by Cardou and Jolicoeur (jan.1997), with 107 references. This review was restricted to the elastic behavior under small deformations, which may include contact conditions, without friction, and possible stick slip behavior. Studies related to more complex situations (multi-layered cables, contact with mechanical elements such as pulleys or clamps, viscoelasticity, fatigue, etc.) are not included.

Experience and good engineering judgment are needed in order to define a good model. The ultimate aim of this review is to identify the best suitable mathematical models irrespective of their field of application to accommodate the more complex situations like friction effects in multi-layered stranded cables under different load conditions like tension, torsion, and bending. Currently, there are three main modeling approaches for strands. They are the first two are the discrete approach and the third one is semi-continuous modeling.

2. ASSUMPTIONS

In many of the earlier theoretical static analysis, however, several simplifying assumptions of questionable validity have been made to obtain analytical or closed from solutions.  The following are the assumptions made by different authors for different models:(1). Relative Wire Size: A strand of a large number of relatively small wires requires a different hypothesis compared with a strand of reasonable size of cores and wires.  The models of contact, internal wire forces and moments and friction are closely related to the ratio of wire size. Such motion may be accommodated either elastically, with some micro slip, or with gross slippage. It is assumed that the center wire is of sufficient size to prevent the outer wires from touching each other. This is generally the case since this tends to minimize the effect of friction in bending. (2). Helix angle variation: The helix angle at any point along the centroidal axis of a wire in a strand is defined as the angle between the tangent vector to the axis and the plane normal to the axis.  For cable designs with regular and long lay in the alternate layers, the critical stresses are relatively smaller when the helix angles are close to /2. Hence such large helix angles are likely to promote longer life span. In contrast, in the wire rope applications for dissipating energy the smaller helix angles in the vicinity of +/3 or -/3 that result in larger contact stresses may be recommended. (3). Helix angle and wire cross-section: For a straight central core wire the helix angle is constant i.e., 900. For a wire with the order of its helical axis greater than one and the helix angle is a periodic function. When helix angle is minimum, the wire cross-section is approximately ellipse. When helix angle is maximum, the wire cross-section is circular. (4). Geometric Structure: A stranded cable is a complex structure made up of layers of thin wires wrapped helically around a central core of a straight wire.  The central core wires are single helices, which remaining wires in outer layers take on the forms of a double helix.  McConnell and Zemke (1981) assumed that the strand can be treated as a single curved line element wrapped on a frictionless cylinder. (5). End Conditions: In all practical applications, since the length of the strand is very long, studies have carried out under “free field”, i.e., hypothesis of long length with respect to diameter.  This assumption makes variations of certain quantities along the length of the wire vanish. (6). Modes of contact: A general property of the contact lead between the wires is that it increases with increasing, decreasing, owing to the straightening of the cable wires (i.e., the helix angle approaching 900). Based on the strain wire diameter and helix angle variation, there are three possible contact modes: (a). Lateral (wire-wire) contact, in which wires in the same layer are in contact, and no (or negligible) contact with adjacent layers. (b). Radial (layer-layer) contact, in which the wires in the same layer do not touch each other, and are in contact only with those in adjacent layers. (c). Mixed (wire-wire and layer-layer) contact, in which both lateral and radial contact occurs.  In practice, one contact has to be selected as the primary one to avoid a statically indeterminate solution, which is mathematically difficult to solve. (7). Material constitutive relations: The cable material is usually assumed to be linearly elastic and isotropic. The time-dependent response and linear viscoelestic behavior will not be considered here. (8). Load conditions: Normally stranded cables are subjected to axial tension, torsion and bending loads.  Among the three the wire axial force is found to have a dominant share over the other two because the major load of the strand is along its axis and the coupling of wire bending and torsion is weak in the lay angle usually adopted for the application of overhead electrical power transmission lines. (9). Internal wire forces and moments: When a strand is loaded, each individual wire is subjected to forces and moments in the normal, bi-normal and tangential (axial) direction involving traction, shear force, twisting and bending.  Strictly speaking, the major load in the normal loading conditions is in the axial direction of the strand and lay angles are small, the wire tensile force in the axial direction is the dominant load. The distribution of other loads, though small, plays a significant role in the local contact and associated slip and energy dissipation. (10). Poisson’s ratio effect (Radial contraction): Kumar and Cochran (1997) proposed a linearized version of Costello’s equation including radial contraction. It is assumed that the cable consists of a single layer of wires and that, if the cable has a central core, either the core is relatively soft in comparison to the cable wires, or it under sized, so that the radial force exerted by the core on the wires may be neglected (Phillips & Costello, 1973). (11). Stress and Strains: The stress and strain analysis of stranded cables were once considered too complex to dealt with by the theory of elasticity (Suslov,1936), and therefore, various assumptions were made regarding the number and types of the loads acting on each wire in the strand in order to obtain a solution.  It is assumed that the strains in the individual wires are small and that the axial and bending response are additive.  In the axial case, the axial force and axial twisting moment are represented as linear combinations of the axial strain and the rotational strain. (12). Bending stiffness: The bending stiffness of the cable will be approximated by a summation of the bending stiffness of the wires in the cable i.e., treating the cable as an assemblage of helical springs.  This is felt to be a reasonable assumption since friction between the wires is neglected. (13). Friction: The equilibrium of each of the constituent helical wires treated separately, although the assumption of no frictional force was kept in tact. It is assumed that the cable is loaded by an axial force and an axial twisting moment, that there are no frictional forces between the wires, and that in the initial unloaded configuration of the cable, the wires are just touching each other (Phillips & Costello, 1973). It is also assumed that the center wire is of sufficient size to prevent the outer wires from touching each other.  This is generally the case since this tends to minimize the effect of friction in bending.  Also, the frictional force depends upon the coefficient of friction and the normal force. (14). Linearity / Non-linearity: In order to simplify the complications of non-linear calculations, it is assumed that the deflection and strain is to be small. (15). Safe working loads and factor of Safety: The maximum load for which a stranded cable is to be used should take into account such associated factors as friction, load caused by tension, twisting and bending, acceleration and deceleration, and, its length to the weight ratio.  Factor of safety for stranded cable usually range form 3 to 4; for wire rope from 5 to 12, where there is the element of hazard to life or property, higher values are used.

## 3. REVIEW OF STRANDED CABLE MODELS

## 3.1. Purely tensile rod or fiber models.

Hruska (1951, 1952, and 1953), has developed this first and simplest model. He made some simplified assumptions that the wires are assumed to be subjected to only tensile forces, no moments, only radial contact is considered, end condition effects are neglected, no radial contraction is considered, friction is not considered and the global strand strain is considered as small. With all these limitations, Hruska has calculated strand interlayer pressure, wire stress and unwinding torque, and also extended this model to multi-stranded wire ropes.

Knapp (1979), has extended Hruska’s work to include the case of cables with compressible core and large strand strains.

Raoof and Hobbs (1988a), have made an experimental study with and orthotropic sheet model (OSM) axial stiffness comparisons and reported test results on 39 mm, 41mm, 51mm, 53mm and 127mm diameter cables. For each cable, Hruska’s fiber model stiffness was calculated and compared with both the experimental and the full-slip OSM values. It was found that the OSM results, which give a lower axial stiffness than the one obtained from the fiber model, are closer to the experimental data.

Strictly speaking, even for a strand under pure axial load, each individual wire subjected to the most general loading, involving traction, shear force, bending and twisting. However, generally, the wire tensile force is, by far and away, the dominant load. Thus, good accuracy is often obtained with fiber models, that is to say, models in which wire bending and twisting stiffness are neglected.

3.2. Discrete rod / helical rod / curved rod / thin rod model (TRM).

## 3.2.1. Introduction.

The basic element of cable is as the name implies a single thin metallic rod. The stranded cable themselves have a center wire that is the axial member around which the individual metallic wires are wrapped helically. It should be mentioned that the helical wires carry the major portion of the load acting on the cable. The main purpose of the core is to provide proper support for the layer wires under loading conditions. In this model where equations are established for individual wire of the strand. The wire bending and twisting is added in this model.

3.2.2. TRM under tension and torsion without friction.

Phillips and Costello (1973), presented a more detailed derivation based on love’s equations for the equilibrium of a curved rod (love, 1944). Separating the cable into thin wires and solving the general nonlinear equations for the bending and twisting of a thin rod subjected to line loads. It is assumed that the cable is loaded by an axial force and an axial twisting moment, that there are no frictional forces between the wires, and that in the initial unloaded configuration of the cable, the wires are just touching each other. Costello and Phillips (1973), assumed for the problem of determining the contact stresses between several initially straight wires which are then twisted and pull is considered.  It should be emphasized that the problem is a nonlinear one due to the presence of large deflections. Large variations of the helix angle are acceptable and smooth contact is again assumed, wire strain is neglected and strand strain arises only from helix angle variations. Machida and Durelli (1973) and Knapp (1979) added wire bending and twisting to this model.

Costello and Phillips (1974), carried out the helical contact line localization by assuming that the wire cross-sections in strand normal section are ellipses, which implies small lay angles, that is less than 30o. Large variations of the helix angle are acceptable and smooth contact is again assumed. Wire stain is neglected and strand stain arises only from helix angle variations.

Costello and Phillips (1976), removed the last hypothesis, and found the curves are slightly nonlinear for practical strain levels. Using the same approach, Costello (1983) subsequently studied a single layer stand with radial wire contact. The equations were linearised by Velinsky et al (1984) for small contraction (Poisson’s ratio only). Phillips et al (1980), evaluated the contact pressure conditions in a double layer strand, with the outer layer in radial contact with the inner layer, and the wires in the latter layer in lateral contact, i.e., no contact with the core. Line contact is assumed between both layers. The contact force per unit length is then transformed into point loads on the outer layer.

Costello and Miller (1980), A theory has been developed to predict the static response of a wire rope consisting of a left lay inner rope and a right lay outer rope. A non rotating rope, under axial load, can be produced by a proper selection of the pitches of the outside and inside rope. The theory is a frictionless one.

Kumar and Cochran (1987), treated separately the equilibrium of each of the constituent helical wires, although the assumption of no frictional force was kept intact. They proposed a linearised version of Costello’s equations including radial contraction. The effect of torsional moment is also incorporated in the analysis along with that of simple tension.

Costello et al (1976, 1985), proposed a much more complex approach, based on love’s equations for curved rods. Machida and Durelli (1973) and Knapp (1979), added wire bending and twisting to this model.

McConnell and Zemke (1982), assumed that the strand can be treated as a single curved line element wrapped on a frictionless cylinder. The axial torsional coupling mechanism of ACSR and ACAR electrical conductors has been described mathematically and measured experimentally.

Conway (1990), studied the ropes subjected to impact loads that send axial and torsional responses up and down the rope. A theory is presented that predicts the contact force between an outer strand and a core strand in a rope (or an outer wire and a core wire in a strand) subjected to an axial impact load. When the contact force remains positive, no separation occurs. If, however, the contact force becomes negative somewhere along the rope, the outer strands will separate from the core strand. When this separation strains the rope material beyond its elastic limit, instability or bird-caging occurs in the form of a permanent deformation.

Jiang (1995), has proposed a general formulation of this theory, including all these aspects, and extended it to more complex situations, such as multi strand ropes. This paper has been discussed by Jolicoeur (1996a) and by Sathikh et al (1996).

Beltran and Williamson (2003) developed computational tools for predicting the response of synthetic-fiber ropes under both monotonic and cyclic loads. In this paper, static tension tests are used to obtain the evolution of the damage index as a function of the strain history. This evolution is computed based on the stiffness ratio between experimental data and simulation of rope response without any source of damage. Numerical simulations of damaged rope behavior compare quite well with experimental data.

Okkenhaug et al, (2003), has been studied to find mooring line safety factors. Design analyses without tension optimization generally leads to higher tension than with optimization. However, simply disallowing line adjustment in design would tend to increase the required strength of the resulting mooring line designs, and thereby raise the safety level.

3.2.3. TRM under tension and torsion with friction.

Huang (1978) studied the contact mode conditions (mixed, radial and lateral) for a 1/6 strand, using the same curved rod equilibrium and constitutive equations. Local contact deformation is neglected whilst the Poisson’s ratio effect is included. Initially, mixed contact (in the unloaded state) is assumed. It is assumed that under axial load, slippage exists between adjacent wires (with friction), with friction between the wire and the core. It is found that lateral contact is lost in all end condition cases (free or blocked rotation). Thus, under these conditions, radial contact seems to be the prevailing case even when no initial gap exists between wires in the layer. The analysis is valid for finite strand extension, but assumes small lay angle.

Utting and Jones (1987a, 1987b), have extended Costello et al’s analysis and development a new mathematical model of a strand was developed to explore the change of helix angle under load, poisons ratio effects in wires, wire flattening under inter wire pressure and the effect of friction between the core and helical wires. They performed a carefully instrument tests on straight single steel strands of seven wire construction subjected to axial loads and with various restrain. The strands have a practical range of lay angles between 9.20 and 170 with core and helical wire diameters of 3.94 and 3.73mm

Ramsey (1990), has attempted to include inter-wire friction in multi-layered strands under going axial loading using a thin rod model. However, this theoretical model of reference has not as yet been verified experimentally and is complex in nature.

Hobbs and Raoof (1996) and Kumar and Botsis (2001), discuss the contact phenomena that occur between fibers in a rope or cable.  These contact phenomena are very similar to the contact forces discussed by Leech (2002) and Labrosse et. al. (1996). Two types of contact occur under tension loading in a spiral stranded rope or cable. The first of these types is the contact between parallel strands in the same layer. Line-contact forces occur when adjacent strands in a spiral stranded rope or cable slide relative to each other, and can be considered to be a large source of energy dissipation when integrated over an entire rope structure. The other type of contact discussed occurs between different layers in a spiral strand and can be called point or trellis contact. Strands in different layers cross at an angle, which produces a point contact rather than a line contact. Trellis contact forces are considered to be much lower than line-contact forces.

Huang and Vinogradov (1996), address the fact that frictional damping in cables is caused mainly by dry friction between fibers, while a small amount is dissipated through individual fiber losses. This is mainly due to the relatively small material viscosity of an individual fiber. Twisting and bending deformations causes slip between separate fibers in a rope or cable. It is this slipping that allows energy to be dissipated.

Costello (1997), many papers have been written on frictional losses in a rope or cable under tension loading. A rope responds to tension loading and unloading by allowing friction between each individual strand in the rope to be released. The friction between strands causes energy to be dissipated, which can in turn dampen a structure. As the displacement between the ends of a rope increases, the individual strand that makes up the rope structure slide against each other and/or a central core.

Banfield and Casey (1998), an evaluation is made on the fiber rope properties for offshore mooring. Varying tensions can result in a change in the mechanical properties of rope as well as fatigue damage. They conducted tension tests on three types of ropes (two aramid types and one polyester type). They concluded that the cyclic loading period, the load range and mean load, material degradation, construction and geometric properties, and the material/scale could influence rope mechanical properties. They also concluded that the fiber rope and the wire rope have very similar performances under axial fatigue.

Banfield and Harley (1998), discuss the dissipation of energy under cyclic loading. Energy is dissipated in part by the friction between individual fibers and the material losses within each fiber.

Hooker (2000), discusses recent developments in braided high-modulus ropes, such as pre-stretching and rope impregnation.  Pre-stretching can increase strength and stiffness significantly. This technique usually involves multiple static load cycles up to a certain percentage of the rope’s breaking strength. Rope impregnation increases the durability of a rope. This involves impregnating the rope with various materials to increase friction between strand fibers.

Labrosse et al. (2000), investigate the frictional damping properties of axially loaded metallic cables consisting of one central wire helically wrapped by one layer of wires.  The damping properties of a cable due to friction are controlled by the contact of internal wires and the geometry of the individual strands.  Tests were conducted so that the outside wires were only touching the central wire core.  Their results proved that the total pivoting friction is a much smaller source of dissipation than the total slip friction. Therefore, whenever inter-wire sliding and inter-wire pivoting or both present; the friction associated with the pivoting can be neglected with respect to cable damping effects.

Leech (2002), explains that friction in synthetic fiber ropes can be categorized as either intra-friction. These two categories can be further broken down into more precise cases of their respective friction modes. In rope construction, the countless fibers that make up the strands are in contact with each other. As tension is applied to a rope, the contact of these fibers becomes more extreme. The energy dissipated by a single fiber due to slipping is very small, but in unison with the numerous other fibers, the energy dissipation may be very significant. These contact forces that develop between individual fibers have been the subjects of several studies. The friction hysteresis related to contact forces is dissipated through material fatigue, heat, and component wear and abrasion.

Zhu Z. H. and Meguid S. A (2006),The goal of the research program is to develop a computational framework and numerical tool aimed at predicting dynamic response of low tension cable systems. The term of "low tension cable" refers to a class of cable systems where the cable is subjected to a small and/or dynamically fluctuating tension which may vanish anywhere along the cable. The broader impact is that the outcome of this research will greatly improve science and industry's ability to model, analyze, and understand a vast array of dynamic problems in an accurate timely manner.

## 3.2.4. TRM under beding withot friction.

Costello and Button (1982), proposed a model in which wires were considered as independent curved rods with no contact restraints by using a more accurate solution for helical spring bending model of Costello (1977). A theory has been developed to predict the static response of wire rope subjected to tension, torsion and bending. The results can be extended so as to include more complex cross sections other than the single lay rope considered herein.

Costello (1983), investigated the axial and bending response of a multi-layered cable. The axial force and the axial twisting moment are represented as linear combinations of the axial strain and the rotational strain. Present model is an extension of the frictionless theory. This is felt to be a reasonable assumption for the case of axial loads. But, in bending, the wires move relative to each other and thus some friction will be developed.

Vinogradov and Atatekin (1986), studied the partial slip due to bending under a completely different set of hypothesis. A strand of finite length is assumed to be clamped at one end and is loaded by a transverse force at the free end. The resulting twisting moment on each wire section is thus periodic and induces wire tension, which is used to evaluate energy dissipation. Axial slip is neglected. This model is discussed by Sathikh and Parthasarathy (1988), a situation has been studied by the same authors (Sathikh and Parthasarathy, 1989; Sathikh, 1989), where the strand is loaded in bending with a sinusoidal transverse displacement. The fiber stress and three wire internal moments are considered and contact assumed to be radial.

Wiek (1986) and Knapp (1988), dealt mainly with the calculation of the radius of curvature of a single helical wires is restricted to the degenerated limiting case of a strand bent into a circular arc.

Raoof (1990) studied the response of a helical strand to an applied bending moment for a given axial mean load. For the critical case near the terminations, the theoretical stiffness formulations describing the slippage between the layers in the strand have been derived in an analytical form, which is then used as an input to the differential equation describing the behavior of individual wires. The theoretical results are of various values as an input to the interwire fretting fatigue analysis of strands. In particular, this model should prove useful for the proper design and interpretation of the very expensive fatigue tests on large-diameter strands.

Goudreau (1990), analyzed when the constant curvature bending is imposed on the core of cable, with or without slipping, a wire may roll on the core. The free field strand bending stiffness was calculated in the no-slip and no-friction conditions. End effects are taken into account and the free field conditions obtained far away from the ends.

## 3.2.5. TRM under bending with friction.

Lutchansky (1969), has introduced a model, based on the same kinematical approach as proposed by Knapp (1983). Infinite friction (no-slip) and Zero friction are considered. Bending and twisting strains are calculated directly from the variation of curvature and twist between the deformed and unreformed helices. In a revised model, instead of using Love’s equilibrium equations, which include unknown contact forces, Knapp (1988) calculates wire-bending stresses from the curvature variation. Thus, his model is purely kinematics. These stresses must be added to the wire tension stress (full-friction or each wire, the resultant moment in the strand axis direction must vanish, which yields a relation between wire bending and twisting moment. Knapp is not interested in global strand bending stiffness, but only in wire stress calculations.

Lanteigne (1985) proposed a model in which the bending moment contribution comes mostly from the fiber effect, calculated using Bernoulli-Euler hypothesis, and also from independent wire bending. Wire twisting is neglected and the bending moments are taken parallel to the strand neutral axis. A model is also proposed for stick-slip transition. In a multiplayer strand, all layers are initially in the no-slip state (wire bending with respect in the strand neutral axis). As the imposed curvature increases, the outer layer reaches a point where it is in a full-slip state, i.e., frictional forces develops between the outer layers and sliding of wires may occur, with the result that the flexural rigidity decreases and the wires bending independently with respect to their own axis. The axial force on the wire (due to bending) vanishes as soon as a layer enters the full-slip regime, and the variations in global strand bending stiffness with imposed curvature yield a staircase-like curve. In addition helically armored cables having a stranded steel core have been analyzed, neglected both the core and wire contact deformation.

Feld et al (1991) have shown that Knapp’s calculation of bending strain should be corrected, because of an oversight in the evaluation of the rotation of the wire centerline principal curvature plane. This corrected bending strain equation has been discussed by Raoof and Huang (1992c).

Raoof and Yu Ping Huang (1991) proposed a theoretical formulation for obtaining upper bounds to single-layer helical strand damping under cyclic bending to a constant radius of curvature. The model employs an alternative inter-wire/inter-layer friction formulation to the traditional rigid-plastic coulomb model. Parametric studies show that the traditional coulomb friction model tends to grossly overestimate cable damping for large radii of curvature such as those found in connection with vortex shedding dynamic instabilities. However, for sufficiently large levels of radii of curvature and cable axial strain, the present theory suggests that for certain ranges of helix angle, increasing helix angle leads to increases in cable damping that can only be predicted with the newly proposed model, which takes no-slip to full-slip inter-wire friction interaction into account.

Sathikh et al (2000) developed a new discrete pre- slip bending response of a strand of helical wires having wire-to-core contacts under the constant curvature bending. Contacts are assumed between the core and the layer wires only (resting lay) with unlimited coulomb friction. Small bending is assumed and hence the difference between the final and initial curvatures and twist and the strains are small and their second order effects are negligible. The core is assumed to be radially rigid. The Poisson effect on wires and core are not considered. Stretch, shear, bending, and twist of a wire in a bent strand are considered together .The effect of wire deformation on the wire curvatures and twist due to the strand bending as discussed by Ramsey (1988) and Wempner (1973) is considered.

Hong et al (2005), developed a mesoscale mechanical model of the bending behaviour of helically wrapped cable under tension. The model accounts for the non-linear dissipative behaviour of the cable arising from the slippage of wires under friction forces. It is shown that the bending stiffness rapidly diminishes with increasing cable curvature, over a range that can be as large as 2 orders of magnitude. The model can be used to assess the static and dynamic response of helically wrapped cables in such applications as conductors in substations and transmission lines subjected to earthquake effects, where significant changes in the cable curvature may occur.

Kenta Inagaki (2005), has been performed a theoretical and experimental study of mechanical properties of electrical cables with multi order helical structure. Relations between applied deformations and local strains in the first order helical structure have been developed. The model is then generalized with a hierarchical approach where the strains at any order helical structure are expressed as functions of strains in the upper order helix under the assumption that all components are sticking to each other. The force balance between the strains and the friction forces is considered. When the cable is exposed to small bending curvature, the slippage of the component is prevented by the frictional force. At this stage, the components of the cable behave as solid beams. Slippage occurs between the components when the tensile force in the components overcomes the frictional force. This state occurs at sufficiently large bending curvatures and results in a variable bending stiffness varying with the magnitude of the applied bending curvature.

Cardou (2006), provides a review of various mechanical models for circular section wire strands which can be found in the literature. Each one of them yields a more or less accurate evaluation of that quantity in terms of the system parameters. As each model has to be based on a set of simplifying assumptions, a classification is proposed. Being a complement as well as an update to a previous paper (Cardou and Jolicoeur, 1997), several relevant references already discussed in that paper, have not been included in this review.

Cardou and Papailiou (2005), developed a mesoscale mechanical model of the bending behavior of helically wrapped cables under tension. The model accounts for the nonlinear dissipative behavior of the cable arising from the slippage of wires under friction forces. It is shown that the bending stiffness rapidly diminishes with increasing cable curvature, over a range that can be as large as 2 orders of magnitude. The model can be used to assess the static and dynamic response of helically wrapped cables in such applications as conductors in substations and transmission lines subjected to earthquake effects, where significant changes in the cable curvature may occur.

Knapp and Xin Liu (2005), proposed a new modeling approach for internally damped, vibrating cables. Instead of the addition of a damping term in the governing cable equation of motion, it is demonstrated that the variation of cable. Flexural rigidity with helical wire slip causes frictional energy dissipation and damping of the cable oscillations. Model results compare favorably with tests performed on a Stockbridge damper cable.

Z.H. Zhu and S.A. Meguid (2007), the flexural damping of wire cable due to the flexural hysteretic influences the dynamic behavior of slacking wire cables significantly. However, the details of the local model, accounting for the flexural hysteresis between the wire strands, are quite challenging to include in large-scale engineering applications. This paper addresses these difficulties by modeling the flexural damping of slacking wire cables using homogenized Rayleigh damping. By using the nonlinear finite element method and high-speed imaging technique, three aspects of the work were examined. First, the mechanical properties of the slacking cable were identified experimentally. Second, a sample cable was fixed at one end and allowed to vibrate freely at the other end. The shapes of the vibrating cable were captured by a high-speed digital camera and processed by photogrammetry. The cable demonstrated a high flexural damping at zero tension and its damping was measured to be as high as 37.7% of the critical damping. Third, the cable was modeled and analyzed using our newly developed nonlinear curved beam element with the Rayleigh damping. The finite element predictions of the cable motion agree well with the experimental measurement. These predictions demonstrate that the new element is capable of describing the dynamic response of the cable and that the Rayleigh damping is sufficient to model the flexural damping of slacking wire cables.

3.2.6. Critical evaluation of thin rod models.

Phillips et al (1973) considered the large changed in helix angle due to loading, and the contact line loads between the individual wires of a cable have been determined for a few representative cases. A general property of the contact load between the wires is that it increases the increasing axial cable force up to a certain point and then decreases, owing to the straightening of the cable wires, when helix angle approaching 900.This-interesting behavior, which seems to prevail for all constant values of the axial cable twisting moment, can only be predicted if the governing equations take into account the change in helix geometry due to loading.

McConnell and Zemke (1982), based on the general agreement between the theoretical and a limited amount of experimental data on the mechanical properties of multi-layered bimetallic conductors, the following conclusions are in order: (a) the constitutive equations for a conductor indicate that torsional and axial deformations are coupled, consequently, an axial deformation causes either an increase or decrease in axial load on the conductor. (b) the axial and torsional stiffness measured depend on the end conditions . Thus, it is easy experimentally to measure AE*, JG, JG* and B was developed. (c) the empirical relations are based on a aluminum of experimental data but can be useful in quickly predicting the physical properties of other sizes of similarly constructed conductors.

Costello (1983) investigated the axial and bending response of a multi-layered cable is presented and it is found that the largest axial tensile stress occurs in the center wire. The axial force and the axial twisting moments are represented as linear combinations of the axial strain and the rotational strain. In his theory, friction is neglected.

Kumar et al (1997), have formed the closed-form expression for critical contact stress has been developed for single strand cables with fibrous cores. Of the two material properties G and , it is only the modulus of rigidity, which is shown to have a strong influence on the resulting level of the contact stresses. Evidently the wire helix angle is rather an important design parameter, which significantly influences these stresses. For cable designs-with regular or lang-lay, the contact stresses are relatively smaller when the helix angles chosen are close to π/2. Hence such large helix angles are likely to promote larger life span. On the other hand, in applications involving the use of the wire ropes for dissipating vibration energy, the smaller helix angles in π/3 or 2π/3 loading to much larger contact stresses may be recommended.

Sathikh et al (2000), a more general discrete thin rod model has been developed to study the pre - slip behavior of a strand layer of helical wires in contact with a core under coulomb stick friction. The simple strand configuration with one layer and a core with wires-to-core contacts under constant curvature free bending, with adequate coulomb friction has deliberately been chosen to enable comparison of results of various models available.

3.3. Semicontinuous models.

## 3.3.1. Introduction.

In this semi continuous modeling approach, each layer of wires in a strand is mathematically represented by an orthotropic hollow circular cylinder whose mechanical properties are chosen to match the behavior of its corresponding layer of wires. This is the method called homogenization in solid mechanics, in which a continuous material replaces a system composed of a large number of identical repetitive elements.

Hobbs and Raoof (1982), was introduced this first orthotropic sheet model (OSM) and it has been described in detail by Raoof (1983). In this model, each layer of wires is replaced with an orthotropic layer, which is helically assumed to be thin, that is to say, in a plane state of stress. As in the case of composite laminates, four elastic constants are necessary. Two of them are directly related to the properties of the wires, considered as fibers. The other two are related to the contact stiffness between adjacent wires in the layer. The normal and tangential stiffness are obtained from contact mechanics equations, using parallel cylinder results. Thus, this is a mixed contact model, in which inlayer lateral contact is considered primary. This approach takes full account of inter-wire/inter-layer friction and contact deformations in multi-layered (large) spiral strands under static monotonic and repeated loading.

Blouin and Cardou (1989), developed the second semi-continuous model and sub sequentially extended by Jolicoeur and Cardou (1994, 1996). In this model, the layer wires are replaced with a cylinder of orthotropic, transversely isotropic material. Cylinder thickness is arbitrary. Thus, one has a three-dimensional model, requiring five elastic constants, rather than four as in the OSM plane stress model. The axes of orthotropy correspond to those of a fiber composite material in which the fiber have the same helix angle as the wires in the corresponding layer (cylindrical anisotropy). Standard linear elastic equations are then applied. In the axial loading case, a set of ordinary differential equations is obtained (one for each layer).The only major difference between the orthotropic sheet model (thin cylinder) and orthotropic cylinder (thick cylinder) model is the first one is considered for two-dimensional and the second one is for three-dimensional calculations.

## 3.3.2. SCM under tension without friction.

Raoof and Hobbs (1988), Raoof (1989, 1990a, 1990b), an extensive series of carefully conducted and large scale tests provided ample support for the various theoretical models, based on SCM concept, for predicting the spiral strand characteristics under axial, torsional, and free bending loading conditions. Most importantly, these models highlighted the first order effects of inter-wire friction and contact deformations on the behavior of spiral strands, especially under cyclic loading, which can have significant practical implications in terms of cable dynamic stabilities Raoof (1991), Raoof and Huang (1993), and axial Raoof (1990) or restrained bending fatigue conditions.

Leach et al (1993), in his recent work assumed the individual helical fibers to carry pure tension, obviously, if wire diameter, d, is a small enough fraction of strand diameter, D, then the wire torque and moment are negligible, as in the extreme case one may quote fiber rope with d/D = 0(10-3).

## 3.3.3. SCM under tension with friction.

Raoof and Hobbs (1988a), considered a mixed contact model, in which in-layer lateral contact is considered as primary. Friction between adjacent wires is also included, with a deformation process evolving gradually from a no-slip to a full-slip stage. The approach is particularly efficient for multi-layer strands. Layers are treated as sequentially, starting from the outer one. The effect of hydrostatic pressure has also been studied by Raoof (1989a).

Raoof (1990), is used previously reported orthotropic sheet theory for obtaining estimates of inter-wire/inter-layer contact stresses throughout realistic pre-tensioned multilayered structural strands. The theoretical interlayer slippage over the individual points of contact between cross-laid layers is addressed, which takes inter-wire friction into account. The match between the theoretical predictions and experimental fatigue data is very encouraging.

Raoof and Kraincanic (1995),The theoretical analysis of a large diameter wire rope, using results from a reported orthotropic sheet model for analyzing the behavior of its constituent helical strands, is reported in this paper. The present model is (unlike available theories on wire ropes) capable of catering to the effects of interwire friction. Experimental results (reported elsewhere) indicate that under axial cyclic loading superimposed on a mean tension, the rope-effective axial stiffness, with its ends fixed against rotation, is not a constant and, in the presence of friction, varies between upper (no-slip) and lower (full-slip) bounds.

3.3.4. SCM under bending without friction.

Jolicoeur and Cardou (1994), a set of equations for an assembly of orthotropic cylinders was developed based on classical elasticity theory. Stress, strain and displacement equations were obtained for the two types of boundary conditions at the cylinder interfaces, that is, no-slip and no-friction. An interesting result of this analysis, which involves no special hypothesis, except that the strain be small, is that plane sections do not remain plane.

Jolicoeur and Cardou (1996), developed a method for obtaining the orthotropic elasticity coefficients of the cylinders. It was shown that the bending stiffness is strongly influenced by the shear modulus. In fact, the whole theoretical range of strand stiffness can be obtained by varying this modulus. It is also found that inter-layer slip exerts an important influence, although not quite as important as the shear modulus. In the previous work (Jolicoeur and Cardou, 1991), it was however, the more complex case of bending, where friction and slip between wires play an important role, was not considered.

## 3.3.5. SCM under bending with friction.

Raoof and Hobbs (1984), considered two basic problems: a) free field bending (far away from strand terminations); and b) termination region bending. In this paper, they proposed a solution for 1) under constant radius bending. In this problem the strand is assumed to be an assembly of coaxial orthotropic cylinders, each having its own modulus of elasticity in the strand axis direction. This modulus is assumed to take one of the extreme values obtained under axial load with full-slip or no-slip. The equivalent strand modulus is obtained using Bernoulli-Euler assumption. Problem 2) was studied by Raoof (1990), based on Lutchansky’s fiber model. Here, the OSM is used to calculate inter-layer pressure, and hence the tangential stiffness.

Raoof and Huang (1992a), with a few modifications of Lanteigne’s slip criterion, attempted an improvement on the termination region-bending problem by including inter-layer slip. Full inter-layer slip is assumed to occur at successively decreasing values of the radius of curvature. The same bending model was subsequently applied marine sheathed cable, that is, cables subjected to uniform hydrostatic pressure (Raoof and Huang, 1992b). It was assumed that a number of cases exist for which neglecting the presence of bending and torsional stiffness of wires was reasonable and could, indeed, lead to considerable simplifications in the theoretical models in which the more important effects of friction plus contact deformations and stresses should be included.

Raoof and Huang (1992), have been carried out parametric studies based on previously reported orthotropic sheet theory on a number of realistic and multilayered helical-strand constructions with widely different strand (and wire) diameters and lay angles. Based on the results, a series of easy to use routines have been recommended which provide a simple means of obtaining estimates of various strand axial and free-bending characteristics such as stiffness and hysteresis of axially preloaded strands experiencing axial or free-bending load perturbations. Due to the presence of interwire friction, axial or free-bending stiffnesses are found to be functions of the external load perturbations:

## 3.3.6. Critical evaluation of SCM.

Hobbs and Raoof (1982), have compared theoretical axial and torsional stiffness predictions using the OSM model with a number of actual cable measurements. A 39 mm diameter, 92 wire steel wire cable has been tested. Axial stiffness was measured for two fixed mean axial loads and for a variable load variation about the mean axial load. The OSM can be made to fit these results with the upper and lower values corresponding to the no-slip and full-slip limits, respectively.

Raoof and Kraincanic (1994), have compared results from the Raoof and Huang (RH) model, and Costello model and have mentioned that the full-slip predictions from RH model for seven-wire strands were not reliable, in particular when one end of the strand was free to rotate.  This is confirmed by the results presented in his results, where the full slip prediction for (GJ) is much closer to Lanteigne’s results (which, as RH model, doesn’t take into account the wire torsion stiffness) than to Costello’s. A discrepancy of the order of 20% persists even when considering elliptical section and no-friction between wires in the RH model (both models then use identical GL values).

## 4. Conclusion.

Using an extensive series of theoretical parametric studies covering a wide range of steel cables (and wire) diameters and lay angles. It is for large diameter strands with number of wires in excess of nineteen can be very different depending on whether thin rod orthotropic sheet models are used. For seven wire strands, thin rod theories and shown to give much more reliable results than the orthotropic sheet approach, especially for cables with free – fixed end conditions. In summary, the models studied in this review, the RH model is simpler and preferred for the strands under tensile and torsional loads. On the other hand, for bending predictions, the JC model should be preferred; because of it has the capability to produce stiffness results in the complete range between theoretical maximum and minimum. It is clear that the maximum existing models are neglecting the presence of bending and torsional stiffness of wires was reasonable and could, indeed, lead to considerable simplification first order effects of inter-wire friction plus contact deformations and stresses should be included.

## FUTURE RESEARCH

Most of the existing models have ignored friction, damping and inter-wire contact deformations and do not meet the required conditions, to predict the actual case adequately. Research required to attempt a more realistic strand model that include all the possible modes of contact, applied to much more complex situations such as multi layered cables.

REFERENCES

1.	Alani A., and Raoof M. (1995) ‘Axial Fatigue Characteristics of Large Diameter Spiral Strands’, Proc. of the 5th International Offshore and Polar Engineering Conference, J.S. Chung, M.Sayed, and A.M. Gresnight (eds.), The Hague, the Netherlands, v.II, pp.260-265.

2.	Alani A., and Raoof M. (1997) ‘Effect of Mean Axial Load on Axial Fatigue Life of Spiral Strands’, Int. J. of Fatigue, v.19, N1, pp.1-11.

3.	Atali M., et al Cardou A. (1995) ‘Energy dissipation and reduction in bending stiffness in axially loaded cable under a constant radius of curvature’, Proc. of Int. Symp. on Cable Dynamics, Liege Belgique, pp.117-124.

4.	Anon – ‘Australian wire rope works Handbook’, AWR Newcastle, N.S.W. Australia.

5.	Bar S. (1976) ‘Centroid of rope forces in multi-rope winding mechanisms; The South African Mech. Eng., 26, pp.53-64.

6.	Bechtoff G. (1969) ‘Stress of cross section of wire rope under Longitudinal Load and Flat transverse pressure’ Draht-welt, v.55, pp.80-87, pp.196-203.

7.	Beeman G.H. (1978) ‘Factors affecting the service life of large diameter wire rope’, report to the U.S. Dept. of energy by pacific Northwest Laboratory, Contract No.ET – 75-C-01-9099.

8.	Beltran J.F and Williamson E.B. (2003) ‘Degradation of Rope Properties under Increasing Monotonic Load’, Int. Symp. on Deepwater Mooring Systems 2003, October 2–3, 2003, Houston, Texas, USA, pp.91-100.

9.	Berglund J.E. and Hofman K.W. (1967) ‘Almost periodic functions’, Springer, Berlin.

10.	Bert C.W. and Stein R.A. (1962) ‘Stress Analysis of wire rope in tension and Torsion’, Wire and wire products, v.37, pp.769-770,772,816.

11.	Besicovitch A.S. (1954) ‘Almost Periodic Functions’.

12.	Blouin F. and Cardou A. (1989) ‘A study of helically reinforced cylinders under symmetric load and application to strand mathematical modeling’, Int. J. Solid Struct., 25(2), pp.189-200.

13.	Butson G.J. (1981) ‘Static and Dynamic analysis of axially loaded wire ropes’, Ph.D. Thesis, University of Illinois, Urbana III.

14.	Beytullah Temel (2004), “Transient analysis of viscoelastic helical rods subject to time-dependent loads”, Int. J. of Solids and Struct., 41, pp.1605-1624.

15.	Conway T.A. and Costllo G.A. (1990) ‘Bird-Caging in Wire Rope’, J. of Eng. Mechanics, v.116, N4, pp.822-831.

16.	Cardou A., Cloutier L., Lanteigne J., et al M’Boup P., (1990) ‘Fatigue Strength Characterization of ACSR Conductors at Suspension Clamps’, Electric Power System Research, v.19, N1, pp.61-71.

17.	Cardou A., Cloutier L., St-Louis M., et Leblond A. (1992) ‘ACSR Electrical Conductors Fretting Fatigue at Spacer Clamps’, Standardization of Fretting Fatigue Test Methods and Equipment, ASTM STP 1159, M. Helmi Attia and R.B. Waterhouse, Eds., American Society for Testing Materials, Philadelphia, pp.231-242.

18.	Cardou A., Leblond A. et Cloutier L. (1993) ‘Suspension clamp and ACSR electrical conductor contact conditions’, ASCE J of Energy Engineering, v.119, N1, pp.19-31.

19.	Cardou A. et Cloutier L. (1997) discussion de ‘On the bending stiffness of transmission line conductors’, par K.O. Papailliou, IEEE Trans, on Power Delivery, v.12, N4, pp.1586-1587.

20.	Cardou A., Dalpe C., et Hardy C. (1997) Fretting fatigue of the Drake ACSR electrical conductor under cyclic bending at suspension clamp’, Comptes rendus, ISF ’97, Int. Symp. on Fretting, Chengdu, China, pp.200-214.

21.	Cardou A. et Jolicoeur C. (1997) ’Mechanical models of helical strands’, Applied Mechanics Reviews, v.50, N1, pp.1-14.

22.	Cardou A., Nailsmith L. and Goudreau S. (2002) ‘Fretting tire under spectrum loading, Application to overhead electrical conductors’, Dept. of genius mech., Laval University; Sm 02-11, pp.16. Presented at the meeting of committee TF22.11.07 of Cigre, Moscow, May 2003.

23.	Cardou A. (2002) ‘The F.I.P. (Fretting Tires) under variable amplitude. Application to the air electric drivers (review of literature)’ Quebec, Mechanical Dept. of engineering, Laval University, Sm 02-11, pp.16.

24.	Cardou A. and Dalpe C. (2002) ‘Static conditions of contact to the DPC between an air electric driver and a grip of standard suspension’ Quebec; Mechanical Dept. of engineering, Laval University, Sm 02-10, pp.19.

25.	Chi M., (1971) ‘Analysis of Operating Characteristics of Strands in Tension Allowing End – Rotation’, Catholic University of America, Report, pp.71-10.

26.	Chi M. (1974) ‘Analysis of multi-wire strands in tension and combined tension and torsion’, Proc. of The seventh south-eastern conference on theoretical and appl. mech. v.7, pp.599-639.

27.	Chi M. (1974) ‘Analysis of Multi-Wire strands in Tension and Combined Tension and Torsion’, Proc. of VII SECTAN, v.7, pp.559-639.

28.	Chien C.H. (1984) ‘Effective length of fractured wires and fatigue analysis of wire rope’, Ph.D. thesis Dept. of Theo. & Appl. Mech., Univ. of Illinois at Urbana – Champaign, pp.104.

29.	Cloutier L., Dalpe C., Cardou A., Hardy C. et Goudreau S. (1999) ‘Studies of conductor vibration fatigue tests, flexural stiffness and fretting behavior’, Comptes rendus Third Int. Symp. on Cable Dynamics, Trondheim, Norvege, pp.197-202.

30.	Committee of wire rope producers/American Iron and Steel Institute, wire rope user’s manual, Washington, 1979.

31.	Chapman R.V. (1908) ‘The Stresses in Wire Ropes due to Bending’, The Engineering Review, v.29, pp.258-269.

32.	Costello G.A. and Phillips J.W. (1974) ‘A more exact theory for twisted wire cable’s’, ASCE, J. Eng. Mech. Div., 102(EM5), pp.1096-1099.

33.	Costello G.A. and Phillips J.W. (1976) ‘Effective modulus of twisted wire cables’ ASCE, J. Eng. Mech. Div., 102(EM1), pp.171-181.

34.	Costello G.A., and Sinha K.S., (1977) ‘Torsional Stiffness of Twisted wire cables’, J. of Eng. Mech. Div., ASCE, pp.766-770.

35.	Costello G.A., and Sinha K.S., (1977) ‘Static Behavior of Wire Rope’, J. of Eng. Mech. Div., ASCE, EM6, pp.1011-1022.

36.	Costello G.A. (1978) ‘Analytical investigation of wire rope’, Appl. Mech. Rev., 31(7), pp.897-900.

37.	Costello G.A. and Miller R.E. (1979) ‘Lay effects of wire rope’, J. Eng. Mech. Div., ASCE, v.105, pp.597-608.

38.	Costello G.A. and Miller R.E. (1980) ‘Static Response of Reduced Rotation Rope’, J. of Eng. Mech. Div., ASCE, EM 4, pp.623-631.

39.	Costello G.A. (1983), ‘Stresses in multilayered cables’, J. Energy Resour. Tech., 105, pp.337-340.

40.	Costello G.A. (1990) ‘Theory of wire rope’, Springer-Verlag, New York.

41.	Costello G.A. and Butson G.J. (1982) ‘Simplified bending theory for wire rope’, ASCE, J. Eng. Mech. Div., 108(EM2), pp.219-227.

42.	Costello G.A. and Phillips J.W. (1983) ‘Stress analysis of wire hoist rope’, Tech. Report, No. UILU – ENG 83 – 6006, Eng. Doc. cent. Univ. of Illinois at Urbana – Champaign, 103 p.

43.	Carstarphen F.C. (1931) ‘Effects of bending wire rope’, Trans ASCE, 57, pp.1439-1466.

44.	Charette F. (1992) ‘Analysis of damping in a vibrating strand’ MSc Thesis, Laval Univ., Quebec, Canada (in French).

45.	Chien C.H. and Costello G.A. (1985) ‘Effective length of fractured wire in wire rope’, ASCE J. Eng. Mech., 111(7), pp.952-961.

46.	Chouinard G. (1994) ‘Energy dissipation at contact points between layers 1 and 2 of a lxnlxn2 helical strand’, MSc Thesis, Laval Univ., Quebec. Canada (in French).

47.	Claren R. and Diana G. (1969a) ‘Dynamic strain distribution on loaded stranded cables’, IEEE Trans Power Appar. Syst., PAS-88 (11), pp.1678-1690.

48.	Costello G.A. (1977) ‘Large deflections of helical spring due to bending’, ASCE, J. Eng. Mech. Div., 103(EM), pp.481-487.

49.	Dalpe C., Nailsmith L., Cardou A. and Goudreau S. (2003) The of knowledge one the fretting behavior in stranded conductors. Dep. of genius mech., Laval University; Sm 03-05, pp.7.

50.	Dalpe C., Goudreau S., Nailsmith L., Cardou A. and Fiset Mr. Rapport (2002) The Alcan company Appraise on the air electric drivers Alcan. Dep. of genius mech., Laval University, Sm 02-08, 98 p.

51.	Deresiewicz H. (1957) ‘Oblique contact of non-spherical elastic bodies’ Appl. Mech., 24, pp.623-624.

52.	De Forest A.V., and Hopking L.W. (1932) ‘Testing of Wire Rope’, Proc. of ASTM, 32, pp.398-412.

53.	Deresiewicz H. (1957) ‘Oblique Contact of Non-spherical Bodies’, J. of Appl. Mech., v.24, pp.623-624.

54.	Drucker D.C. and Tachau H. (1945) ‘A new design criterion for wire rope’ Appl. Mech., 67, pp.A33-A38.

55.	Durelli A.J., Machida S. and Parks V.S. (1962) ‘Strains and displacements on a steel wire strand’, Naval Engineers J., pp.85-93.

56.	Durelli A.J. and Machida S. (1973) ‘Response of epoxy oversized models of strands to axial and torsional loads’ Exp. Mech., 13, pp.313-321.

57.	Durelli A.J., Machida S. and Parks V.J. (1972) ‘Strains and displacements on a steep wire strand’, Naval Engineers J., pp.85-93.

58.	Dull G. and Parkinson R. (1983) ‘Warning: Hand – spliced slings and rotating loads – a bad combination, wire rope news and sling technology’, pp.18-22.

59.	Egeseli Eugin A., Fleming John F. (1976) ‘Dynamic Behaviors of Cable Stayed bridges’, Proc. of Int. Symp. on Earthquake Structural Engineering, St. Louis. Pub. By M.O. Dept. of Civil Engineering, Rolla, VI, pp.59-67.

60.	Elata D. and Eshkenazy R. (2004) “The mechanical behavior of a wire rope with an independent wire rope core”, Int. J. of Solids and Struct., 41, pp.1157-1172.

61.	EPRI (1979) ‘Transmission Line Reference Book’, Electric Power Research Inst. Palo-alto, CA.

62.	Fang J. and Lyons G.J. (1996) ‘Structural damping of tensioned pipes with reference to cables’, J. Sound Vib., 193(4), pp.891-907.

63.	Feld G. Reuben R.L. and Owen D.G. (1991) ‘Power cables and umbilical – conductor strain under pure bending’, Proc. 1st Int. Offshore Polar Eng Conf., Edinburgh,UK, pp.228-235.

64.	Faraji A., Gakwaya A. et Cardou A. (2003) ‘A boundary element mathematical programming method for solving 3D elastic contact problems with friction’, Comptes rendus sur cd –rom, 6 eme Colloquies National en Calculi des Structures, Glens, France 20-23, 8 p.

65.	Faraji A., Cardou A. et Gosseling C. (1996) ‘A study of edge effects on some contact problems’, Proc. Mechanics in Design Conf., Toronto, pp.289-298.

66.	Faraji A., Cardou A. et Gakwaya A. (1999) ‘The effect of an arbitrarily directed tangential force on elastic contacting bodies’, ASCE, J. of Engrg. Mech., Tech. Note, v.125, N11, pp.1324-1326.

67.	Fotsch P.D. (1983) ‘Analysis of complex wire rope’, Dept. of Theory and Appl. Mech., Univ. of Illinois – Urbana, III, T & A.M., Report N458.

68.	Gakwaya A., Lambert D. et Cardou A. (1992) ‘A boundary element and mathematical formulation for 3D frictional contact problems’, Int. J. for computers and structures, v.42, N3, pp.341-353.

69.	Gakwaya A., Kong X.A. et Cardou A. (1994) Boundary element and mathematical programming techniques for frictional contact problems’, Proc. of CSCE 1994 Engineering Mechanics Symposium, v.IV, Winnipeg, Man., pp.321-326.

70.	Gibson P.T., Cress H.A. Kaufman W.J. and Gallant W.E. (1969) ‘Torsional properties of wire rope’, ASME, paper 69 – DE – 34.

71.	Gibson P.T., Karleen R.E. and Cress H.A. (1971) ‘The Continuation of Analytical and Experimental Investigation of Aircraft Arresting Gear Purchase Cable’, Final Report AD 905-835, prepared by Bastille’s Columbus Laboratories for the Naval Air Engineering Center.

72.	Goudreau S., Nailsmith L. and Cardou A. (2002) ‘Expertise on an earth wire Alcan’, Dep. of genius mech., Laval University, Sm 02-12, pp.24.

73.	Goudreau S., Nailsmith L. and Cardou A. (2001) Fatigue tests one stranded conductors return of experiment. Cigre WG-11 28th Meeting, Quebec, Paper 22-01, 27 p.

74.	Goudreau S. (1990) ‘Study of helical strands in bending’, Univ Laval. Ste-Foy, QC, Canada (in French).

75.	Goudreau S. and Cardou A. (1993) ‘Flexural testing of an epoxy oversized strands model under traction’, Exp Mech., 33, pp.300-307.

76.	Gopalan T.V. and Nagaphushana G.R. (1984) ‘Some Aspects of Fatigue Stresses in ACSR, EHV Transmission Line Cables’, Paper presented in the Conference and Workshop of EHV Technology, Bangalore, pp.5-18.

77.	Hruska F.H. (1951) ‘Calculation of Stresses in Wire Ropes’, Wire and Wire Products, v.26, pp.786-767, 799-801.

78.	Hruska F.H. (1952) ‘Radial Forces in Wire Ropes’, Wire and Wire Products, v.27, pp.459-463.

79.	Hruska F.H. (1953) ‘Tangential Forces in Wire Ropes’, Wire and Wire Products, v.28, pp.455-460.

80.	Hadj-Mimoune A., Cardou A. and Chebair A. (1993) ‘Free constant curvature bending of axially preloaded strands’, Trans. Can. Soc. Mech. Eng., 17(3), pp.325-350.

81.	Hadj-Mimoune A. and Cardou A. (1994) ‘A model for the estimation of damping in helical strand under bending vibration’, in Proc. XXth Leeds Lyon Symp on Trib. Lyon, France. D. Dawson et al (ed.).,Elsevier Sci. BV, Amsterdam, Netherlands, pp.373-387.

82.	Hardy C. (1990) ‘Analysis of self – damping characteristics of stranded cables in transverse vibration’ in Proc. Can. Soc. Mech. Eng. Forum, Toronto ON Canada, pp.117-122.

83.	Hardy C., Leblond A., Goudreau S. and Cloutier. L. (1995) ‘Review of models on self damping of stranded cables in transverse vibrations’ in Proc. Int. Symp. Cable Dyne, Liege, Belgium, 1995, pp.61-68.

84.	Hobbs R.E. and Raoof M. (1982) ‘Inter-wire slippage and fatigue prediction in stranded cables for TLP tethers’ in Proc. 3rd Int. Conf. Behavior Offshore Struct., C. Chryssostomidis and J.J. Connor (eds.), Hemisphere Pub/McGraw-Hill, New York, pp.77-92.

85.	Hobbs R.E. and Raoof M. (1982) ‘Inter-wire Slippage and Fatigue Prediction in Stranded Cables for TLP Tethers’ in ‘Behavior of Offshore Structures’, Chryssostomidis C. and Connor J.J. (eds.), Hemisphere Publishing/McGraw-Hill, New York, v.2, pp.77-99, ISBN 0-89116-343-3.

86.	Hobbs R.E. and Ghavami K. (1982) ‘The Fatigue of Structural Wire Strands’, Int. J. of Fatigue, v.4, pp.69-72.

87.	Hobbs R.E. and Smith B.W. (1983) ‘The Fatigue Performance of Socketed Terminations to Structural Strands’, Proc. Inst. of Civil Engineers, v.75, pp.35-48.

88.	Hobbs R.E. and Raoof M. (1983) ‘Predictions of the Elastic Properties of Large Strand and Cables’, Wire Industry, v.52, N163, pp.39-43.

89.	Hobbs R.E. and Raoof M. (1983) Discussion on ‘Simplified Bending Theory for Wire Rope’, by Costello G.A. and Boston G.J., J. of Eng. Mech. Div., American Society of Civil Engineers, v.109, N2, pp.662-664.

90.	Hobbs R.E. and Raoof M. (1984) ‘Hysteresis in Bridge Strand’, Proc. Inst. of Civil Engineers, Part II, v.77, pp.445-464.

91.	Hobbs R.E. and Raoof M. (1986) ‘The Behavior of Large Spiral Strands’, Proc. of the 5th International Offshore Mechanics and Arctic Engineering Symposium, American Society of Mechanical Engineers, Tokyo, Japan, v.3, pp.543-549.

92.	Hobbs R.E. and Raoof M. (1994) ‘Mechanism of Fretting Fatigue in Steel Cables’, Int. J. of Fatigue, v.16, pp.273-280.

93.	Hobbs R.E. and Raoof M. (1996) ‘Behavior of Cables Under Dynamic or Repeated Loading’, J. of Constructional Steel Research, v.39, N1, pp.31-50.

94.	Hruska FH(1951), ‘Calculation of stresses in wire ropes’, Wire and Wire Prod 26(9), PP 766-767, 799-801.

95.	Hruska F.H. (1952) ‘Radial forces in wire ropes’, Wire and Wire Prod., 27(5), pp.459-460.

96.	Huang N.C. (1978) ‘Finite extension of an elastic strand with a central core’, J Appl. Mech., 45(4), pp.852-857.

97.	Huang X. and Vinogradov O. (1994) ‘Analysis of dry friction Hysteresis in a cable under uniform bending’, Struct. Eng. Mech., 2(1), pp.63-80.

98.	Hertz H. (1896) Miscellaneous papers, Macmillan, London, pp.146-183.

99.	Hobbs R.E. and Ghavami K. (1982) ‘The fatigue of structural wire strands’, Int. J. of Fatigue, 4(2), pp.69-72.

100.	Huang N.C. (1977) ‘On the flexure of elastic tow filament yarns’, Textile Res. J., 47(1), pp.73-76.

101.	Hurty A. and Walter C. (1967) (University of California), Rubinstein and Noshe F., (University of California) ‘Dynamics of Structures’, printed by prentice Hall of India Private Limited, New Delhi.

- Jiang W. (1995) ‘General formulation of the theories of wire ropes’, J. Appl. Mech., 62, pp.747-755.

- Jolicoeur C., Goudreau S., Cardou A. and Nailsmith L. (2002) Fatigue tests of driver ACSR Crow with amplitude varying according to a distribution of Raleigh Dept of genius mec., Laval University, Sm 01-07, pp.36.

- Jolicoeur C. (1996a) ‘Discussion of A general formulation of the theories of wire ropes’, J. Appl. Mech., 63, pp.1053.

- Jolicoeur C. (1996b) ‘Comparative study of two semi continuous modes for wire strand analysis’, ASCE J. Eng. Mech., accepted for publication.

- Jolicoeur C. and Cardou A. (1991) ‘Numerical comparison of current mathematical models of twisted wire cables under axi-symmetric loads’, J. Energy Resources Tech., 113(4), pp.241-249.

- Jolicoeur C. and Cardou A. (1994) ‘Analytical solution for bending of coaxial orthotropic cylinders’, ASCE J. Eng. Mech., 120(12), pp.2556-2574.

- Jolicoeur C. and Cardou A. (1996) ‘Semi continuous mathematical model for bending of multilayered wire strands’, ASCE J. Eng. Mech., 122(7), pp.643-650.

- Jolicoeur C. and Cardou A. (1994) ‘Modelisation semi continue des conductors electrocutes aeries’, Comptes rendus, 12em colloquia ATM, Montreal, pp.205-214.

- Knapp R.H. (1979) ‘Derivations of a new stiffness matrix for helically armored cables considering tension and torsion’, Int. J. Numer. Methods Eng., 14, pp.515-529.

- Knapp R.H. (1983) ‘Simple bending models for helically armored cables’ in Proc. 2nd Int. Offshore Mech. Arctic Eng. Symp., J.S. Chund and V.J. Lunardini (eds.), ASME, New York, pp.360-364.

- Knapp R.H. (1988) ‘Helical wire stresses in bent cables’, J. Offshore Mech. Arctic Eng., 110, pp.55-61.

- Kraus M. and Hagedorn P. (1991) Acolian vibrations: wind energy input evaluated form measurements on air energized transmission line’ IEEE Trans Power Delivery, 6(3), pp.1264-1270.

- Kumar K. and Cochran J.E. (1987) ‘Closed form analysis of elastic deformations of multilayered strands’, J. Appl. Mech., 54, pp.898-903.

- Kunoh T. and Leech C.M. (1985) ‘Curvature effects on contact position of wire strands’, Int. J. Mech. Sci., 27(7), pp.465-470.

- Karamchetty S.D.S.R. (1978) ‘Some Geometrical characteristics of wires in wire ropes’, Proc. of the ninth sect Am, Developments in Theoretical and Applied Mechanics, v.9, pp.519-541.

- Karamchetty S.D.S.R. (1979)‘Sections of a Torus – Application to contact stress problems in wire ropes’, Trans. ASME Vol.100, PP 543-552.

- Karamchetty, S.D.S.R. and Yuen W.Y. (1979) ‘Contact problems in wire ropes’, Trans ASME, v.101, pp.702-710.

- Knapp and Xin Liu (2005) ‘Cable Vibration Considering Interlayer Coulomb Friction’, Int. J. of Offshore and Polar Engineering (ISSN 1053-5381), v.15, N3, pp.229-234.

- Kong X.A., Gakwaya A., Cardou A. et Cloutier L. (1993) ‘A unified BEM formulation for elastio-plastic frictional contact problems by particular integrals and mathematical programming’, Eur. J. of Mechanics (A), v.12, N4, pp.537-566.

- Kong X.A., Gakwaya A., Cardou A. et Cloutier L. (1992) ‘A numerical solution of general frictional contact problems by the direct boundary element and mathematical programming approach’, Int. J. for computers and structures, v.45, N1, pp.95-112.

- Kong X.A., Gakwaya A. et Cardou A. ‘A direct solution to the BEM and Mathematical Programming Approach for Frictional Constant Contact Problems’ in Boundary Elements XIII, C.A. Brebbia et G.S. Gipson (eds.) Computational Mechanics Publications et Elsevier Applied Science, 13th Boundary Element Method International Conference, BEM 13, Tulsa, Oklahoma, pp.677-688.

- Kumar K. and Cochran J.E. (1990) ‘Analytical estimation for static deformation of wire ropes with fibrous core’, Trans., ASME, v.57, pp.1000-1003.

- Kumar K. and Botsis J. (2001) ‘Contact stress in multi layered strands under tension and torsion’, J. of Appl. Mech., v.68, pp.432-440.

- Langhaar H.L. (1980) ‘Dimensional analysis and theory of models’ Huntington N.Y. Robert E. Krieger Publishing company, 166 p.

- Lanteigne J., Cardou A. et Cloutier L. (1985) ‘Fatigue Tests on a Typical ACSR conductor’, CEA Conductor Vibration Workshop, Montreal Canadian Electrical Association, Engineering and Operating Division, Transactions, v.24, 18 p.

- Leech C.M., Hearle J.W.S., Overington M.S., Ban field S.J. (1993) ‘Modeling tension and torque properties of fiber ropes and splices’, Proc. of The Third Int. Offshore and Polar Engg. Conf., v.II, pp.370-376.

- Leissa A. (1959) ‘Contact stress in wire ropes’, Wire and Wire Products, v.34, pp.307-314, 372-373.

- Li. G., Goudreau S., Cardou A. et Cloutier L. (1998) ‘Energie dissipee par friction dans un toron 1xN1 x N2 sous flexion selon differents modeles de complaisance tangentielle’, Comptes rendus du Forum SCGM, Toronto, v.2, pp.46-52.

- Lubkin J.L. (1962) ‘Contact problems’, Handbook of Engg. Mech., ed., Flugge W., McGraw-Hill, New York.

- Lanteigne J (1985) ‘Theoretical estimation of the response of helically armored cables to tension, torsion and bending’, J. Appl. Mech., 52, pp.423-432.

- Le Clair R.A. (1989) ‘Upper bound to mechanical power transmission losses in wire rope’, ASCE, J. Eng. Mech., 115(9), pp.2011-2019.

- Le Clair R.A. (1991) ‘Axial response of multilayered strands with compliant layers’, ASCE, J. Eng. Mech., 117(12), pp.2884-2903.

- Le Clair R.A. and Costello G. (1988) ‘Axial, bending and torsional loading of a strand with friction’, J. Offshore Mech. Arctic Eng., 110, pp.38-42.

- Love AEH (1944) ‘Mathematical Theory of Elasticity’, Dover Pub, New York.

- Lutchansky M. (1969) ‘Axial stresses in armor wires of bent submarine cables’, J. Eng. Ind., 91, pp.687-693.

- Machida S. and Durelli A.J. (1973) ‘Response of a strand to axial and torsional displacements’, J. Mech. Eng. Sci., 15(4), pp.241-251.

- McConnell K.G. and Zemke W.P. (1980) ‘Measurement of Flexural stiffness of multi-stranded electrical conductors while under tension’, Exp. Mech., 20(6), pp.198-204.

- McConnell K.G. Zemke W.P. (1982) ‘Model to predict the coupled axial torsion properties of ACSR electrical conductors’, Exp. Mech., 22(7), pp.237-244.

- Morgan Stern M.H. et al (1980) ‘Wire rope improvement program’, fiscal years 1979-1980, Interim report to the U.S. Dept. of Energy by Pacific North West Laboratory, contract No. DE-A-106076RLD 1830.

- Noiseux D.U. (1992) ‘Similarity laws of the internal damping of stranded cables in transverse vibrations’, IEEE Trans. Power Delivery, 7(3), PP pp.817-823.

- Nowak G. (1974) ‘Computer design of electromechanical cables for ocean applications’, Proc 10th Marine Tech Soc Conf., Washington DC, 293-305.

- Nilson Barbieri and Paulo Rogerio Novak (2004) “Experimental identification of damping”, Int. J. of Solid and Struct., 41, pp.3585-3594.

- Okkenhaug S., Fylling I., Haver S. and Marthinsen T. (2003) ‘The Effect of Weather Dependent Line Tension Optimisation in Design’, Int. Symp. on Deepwater Mooring Systems, Houston, Texas, USA, pp.271-285.

- Ouaki B., Goudreau S., Cardou A. and Fiset M. (2003) ‘Fretting Fatigue analysis of aluminium conductor wires near the suspension clamp; metallurgical and fracture mechanics analysis’, J. Strain Analysis, 38(2), pp.133-147.

- Ouaki B., Goudreau S. and Cardou A. (2003) ‘Experimental and theoretical analysis of fretting tiredness ramming of conductor wires near the suspension clamp using fracture mechanics’, 6th Congress of mechanics of the Moroccan Company of Mechanical Sciences; Tangier, Morocco, 3 p.

- Owada S. (1952) ‘Calculation of tensile and torsonal stiffness of single-lay cables’, Proc. of |The Second Japan National Cong. for Appl. Mech., pp.159-164.

- Papailiou E.O. (1996) ‘Bending stiffness of transmission line conductors’, IEEE/PES Summer Meeting, Denver CO, Paper No 96-SM-444-0-PWRD, pp.8.

- Phillips J.W. and Costello G.A. (1973) ‘Contact stresses in twisted wire cables’, ASCE, J. Eng. Mech. Div., 99(EM2), pp.331-341.

- Phillips J.W., Miller R.E. and Costello G.A. (1980) ‘Contact stresses in a straight cross-lay wire rope’, Proc. 1st Annual Wire Rope Conf., Denver, pp.177-199.

- Poffenberger J.C. and Swart R.L. (1965) ‘Differential displacement and dynamic conductors strain’, IEEE Trans. Power Appar. Syst., PAS-84(4), pp.281-289.

- Phillips J.W. and Costello G.A. (1972) ‘Large deflections of Impacted Helical springs’, J. of the Acoustical Soc. of Amer., v.51, N3, part 2, pp.967-973.

- Ramsey H. (1988) ‘Theory of thin rods with application to helical constituent wires in cables’, Int. J. Mech. Sci., 30(8), pp.559-570.

- Ramsey H. (1990) ‘Analysis of inter-wire friction in multilayered cables under uniform extension and twisting’, Int. J. Mech. Sci., 32(8), pp.709-716.

- Ramsey H. (1991) ‘Localized effect of clamp or socket and connections on helical wires in multilayered cables’, Int. J. Solid Struct., 28(6), pp.779-790.

- Raoof M. (1983) ‘Inter-wire contact forces and the static, hysteretic and fatigue properties of multi-layer structural strands’, PhD Thesis Imperial Col. of Sci. and Tech., London.

- Raoof M. and Hobbs R.E. (1984) ‘Bending of spiral strand and armored cables close to terminations’, J. Energy Resource Tech., 106, pp.349-355.

- Raoof M. and Hobbs R.E. (1988) ‘Torsion Tests on Large Spiral Strands’, J. of Strain Analysis, Inst. of Mechanical Engineers, v.23, N2, pp.97-104.

- Raoof M. and Hobbs R.E. (1988a) ‘Analysis of multilayered structural strands’, Proc. Inst. Civil Eng. Mech., 114(7), pp.1166-1182.

- Raoof M. and Hobbs R.E. (1988b) ‘Torsional stiffness and Hysteresis in spiral strands’, J. Strain Anal. Eng. Des., 23(2), pp.93-107.

- Raoof M. and Hobbs R.E. (1989) ‘Torsional stiffness and Hysteresis in spiral strands’, Proc. Inst. Civil Eng., Part II, v.87, pp.501-515.

- Raoof M. and Hobbs R.E. (1989) ‘Tangential Compliance of Rough Elastic Bodies in Contact’, J. of Tribology, American Society of Mechanical Engineers, v.111, pp.726-729.

- Raoof M. (1989) ‘Free Bending Tests on Large Spiral Strands’, Proc. of the Inst. of Civil Engineers, Part II, v.87, pp.605-626.

- Raoof M. (1989a) ‘Theoretical effect of external pressure on spiral strand’, Proc. Inst. Civil Eng., Part II, v.87, pp.113-118.

- Raoof M. (1990) ‘Free bending of spiral strands’, ASCE, J. Eng. Mech., 116(3), pp.512-530.

- Raoof M. (1990) ‘Comparison Between the Performance of Newly Manufactured and Well-used Spiral Strands’, Proc. of the Inst. of Civil Engineers, Part II, v.89, pp.103-120.

- Raoof M. (1990) ‘Sheathed Spiral Strands in Deep Water Applications’, Proc. of the 9th Int. Conf. on Offshore Mechanics and Arctic Engineering, American Society of Mechanical Engineers. Houston, TX, USA, v.1, Part B, pp.613-622.

- Raoof M. (1990) ‘Effect of Hydrostatic Pressure on Strand Behavior’, J. of Strain Analysis, Inst. of Mechanical Engineers, v.25, N2, pp.75-84.

- Raoof M. (1990) ‘A Multi-Contact Problem’, Proc. of the 9th Int. Conf. on Experimental Mechanics, v.1, Technical university of Denmark, Lyngby, Copendhagen, Denmark, pp.103-111.

- Raoof M. (1990) ‘Axial Fatigue of Multi-layers Strands’, J. of Engineering Mechanics, American Society of Civil Engineers, v.116, N10, pp.2083-2099.

- Raoof M. (1990) ‘Simple Formulae for Spiral Strands and Multi-Strand Ropes’, Proc. of the Inst. of Civil Engineers, Part II, v.89, pp.527-542.

- Raoof M. and Huang Y.P. (1991) ‘Upper bound prediction of cable damping under cyclic bending’, ASCE, J. Eng. Mech., 117(12), pp.2729-2747.

- Raoof M. (1991) ‘Axial Fatigue Life Prediction of Structural Cables from First Principles’, Proc. of the Inst. of Civil Engineers, Part II, v.91, pp.19-38.

- Raoof M. (1991) ‘Cable Fatigue Prediction in Offshore Applications’, Proc. of the 10th Int. Conf. on Offshore Mechanics and Arctic Engineering, American Society of Mechanical Engineers, Stavanger, Norway, v.III, Part B, pp.403-411.

- Raoof M. (1991) ‘Cable Behavior under Various Loading Conditions”, Structural Engineering Review, v.3, N2, pp.89-90.

- Raoof M. (1991a) ‘Methods of analyzing large spiral strands’, J. Strain Anal. Eng. Des., 26(3), pp.165-174.

- Raoof M. (1991b) ‘Prediction of axial damping in spiral strands’, J. Strain Anal. Eng. Des., 26(4), p.221-230.

- Raoof M. (1991c) ‘Wire recovery length in a helical strand under axial – fatigue loading’, Int. J. Fatigue, 13(2), pp.127-132.

- Raoof M. (1992) ‘Free-bending fatigue life estimation of cables at points o fixity’, ASCE, J. Eng. Mech., 118(9), pp.1747-1764.

- Raoof M. (1992) ‘Wire Recovery Length in Steel Cables’, Proc. of The 11th Int. Conf. on Offshore Mechanics and Arctic Engineering, American Society of Mechanical Engineers, Calgary, Canada, v.III, Part B, pp.449-458.

- Raoof M. (1992) ‘A Critical Review of Draft API Recommended Practice 2FPI Regarding Fatigue Life Estimation of Moorings’, Proc. of the 11th Int. Conf. on Offshore Mechanics and Arctic Engineering American Society of Mechanical Engineers, Calgary, Canada, v.III, Part B, pp.521-532.

- Raoof M. and Huang Y.P. (1992) ‘Bending Stiffness and Hysteresis of Sheathed Spiral Strands’, Proc. of The 2nd Int. Offshore and Polar Engineering Conference, M.S. Triantafyllou, J.S. Chung, K.Karal and A.L. Tunik (eds.), San Francisco, USA, v. II, pp.369-379.

- Raoof M. and Huang Y.P. (1992) ‘Free Bending Hysteresis in Spiral Strands’, Proc. of The 2nd Int. Offshore and Polar Engineering Conference, M.S. Triantafyllou, J.S.Chung, K. Karal and A.L. Tunik (eds.), San Francisco, USA, v.II, pp.380-391.

- Raoof M. (1992) ‘Free Bending Fatigue Life Estimation for Cables at Points of Fixity’, J. of Eng. Mech., American Society of Civil Engineers, v.118, N9, pp.1747-1764.

- Raoof M. (1992) ‘Design Recommendations for steel cables’, Structural Engineering Review, v.4, N3, pp.223-233.

- Raoof M. and Huang Y.P. (1992) ‘Simplified Methods for Analyzing Steel Strands’, The Structural Engineer, Institution of Structural Engineers, v.70, N22, pp.390-397.

- Raoof M. and Huang Y.P. (1992a), ‘Free bending characteristic of axially preloaded spiral strands’, Proc. Inst. Civil Eng. Struct. & Build, 94, pp.469-484.

- Raoof M. and Huang Y.P. (1992b) ‘Free bending characteristics of sheathed spiral strands under cyclic loading’, J. Strain Anal. Eng. Des., 27(4), pp.219-226.

- Raoof M. and Huang Y.P. (1992c) ‘Wire stress calculation helical strands undergoing bending’, J. Offshore Mech. Arctic, pp.212-219.

- Raoof M. and Huang Y.P. (1992) ‘Axial and Free Bending Analysis of Spiral Strands Made Simple’, J. of Eng. Mech., American Society of Civil Engineers, v.118, N12, pp.2335-2351.

- Raoof M. and Huang Y.P. (1992) ‘Wire Recovery Length in Suspension Bridge Cable’, J. of Structural Engineering, American Society of Civil Engineers, v.118, N12, pp.3255-3267.

- Raoof M. and Huang Y.P. (1992) ‘Simple Methods for Estimating Various Sheathed spiral Strand Bending Characteristics’, Proc. of the Institution of Civil Engineers, Structures and Buildings, v.94, pp.485-500.

- Raoof M. (1993) ‘Influence of Inter-wire Contact Forces on the Overall Behavior of Spiral Strands’, Workshop on Length Effect of Fatigue of Wires and Strands, organized by International Association for Bridge and Structural Engineering (IABSE), Sept., 1992, El Paular, Madrid, Spain, Proceeding published by IABSE, Zurich, Switzerland, Report 66, PP 279-291. ISBN3-85748-080-7.

- Raoof M. (1993) ‘Design of Steel Cables Against Free Bending Fatigue at Terminations’, The Structural Engineer, Institution of Structural Engineers, v.71, N10, pp.171-178.

- Raoof M. and Huang Y.P. (1993), ‘Lateral vibrations including structural damping’, Proc. Inst. Civil Eng. Struct., pp.123-133.

- Raoof M. and Huang Y.P. (1993) ‘Effect of Non-Linear Structural Damping on Cable Lateral Vibrations’, Proc. of The 3rd International Offshore and Polar Engineering Conference, J.S. Chung, K. Karal, M.S. Triantafyllou and R.W. Frederking (eds.), Singapore, v.II, pp.435-444.

- Raoof M. (1993) ‘Design of Sheathed Spiral Strands Against Free Bending Fatigue at Terminations’, J. of Strain Analysis, Institution of Mechanical Engineers, v.28, N3, pp.163-174.

- Raoof M. Huang Y.P. and Pithia K. (1993) ‘Axial – Torsional Coupling of Spiral Strands Under Impact Loading’, Proc. of the Institution of Civil Engineers, Structures and Buildings, v.99, pp.371-374.

- Raoof M. and Huang Y.P. (1993) ‘Cyclic Bending Characteristics of Sheathed Spiral Strands in Deep Water Applications’, Int. J. of Offshore and Polar Engineering, v.3, N3, pp.189-196.

- Raoof M. (1993) ‘An Insight into the Mechanisms of Inter-wire fretting in Spiral Strands’, Proc. of The organization Internationals pour I’ Etude de I’ Endurance des cables (OIPEEC) Round Table Conference, L. Wiek (ed.), Delft University, Delft, The Netherlands, ISBN 90-370-0091-6.

- Raoof M. and Kraincanic L. (1993) ‘Recovery Length in Sheathed Spiral Strands in Deep-Water Platform Applications’, Int. J. of Fatigue, v.15, N6, pp.485-492.

- Raoof M. and Kraincanic I. (1994) ‘Critical examination of various approaches used for analyzing helical cables’, J. Strain Anal. Eng. Des., 29(1), pp.43-55.

- Raoof M. and Kraincanic L. (1994) ‘Determination of Recovery Length in Spiral Strands’, Proc. of The 13th Int. Conf. on Offshore Mechanics and Arctic Engineering, American Society of Mechanical Engineers, Houston, TX, USA, v.III, pp.271-280.

- Raoof M., Huang Y.P. and Pithia K.D. (1994) ‘Response of Axially Preloaded Spiral Strands to Impact Loading’, Computers and Structures, v.51, N2, pp.125-135.

- Raoof M. and Huang Y.P. (1994) ‘Estimation of Spiral Strand Bending Fatigue Life’, Proc. of the Seventh Int. Conf. on Behavior of Offshore Structures (BOSS ’94), C. Chryssostomidis (ed.), Pergamon, v.2, M.I.T., Cambridge, M.A., USA, pp.203-212, ISBN 008 041916X.

- Raoof M. (1994) ‘Prediction of Lateral Vibrations and Associated Fatigue Problems of Bridge Cables’, Proc. of the Deauville Conf. on Cable – Stayed and Suspension Bridges, organized by the Int. Association for Bridge and Structural Engineering (IABSE), Deauville, France, v.II, pp.465-474, ISSN 0761-3458.

- Raoof M. and Hobbs R.E. (1994) ‘Analysis of Axial Fatigue Data for Wire Ropes’, Int. J. of Fatigue, v.16, pp.493-501.

- Raoof M. and Kraincanic L. (1994) ‘Axial / Torsional Coupling of Sheathed Spiral Strands in Deep Water Applications’, Proc. of the Inst. of Civil Engineers, Structures and Buildings, v.104, pp.377-390.

- Raoof M. (1994) ‘Free Bending Fatigue Prediction of Steel Cables with the Effect of Inter-wire Fretting taken into account’, Fretting Fatigue, ESIS 18, Mechanical Engineering Publications, London, pp.267-281, ISBN 08298 9407.

- Raoof M. (1994) Discussion on “Estimation of Damping Ratio of Cable-Stayed Brides for seismic Design”, by Kazuhika Kawashima, et al., J. of Structural Engineering, American Society of Civil Engineers, v.120, N8, pp.2648-2550.

- Raoof M. and Kraincanic L. (1995) ‘Analysis of Large Diameter Steel Ropes’, J. of Eng. Mech., American Society of Civil Engineers, v.121, N6, pp.667-675.

- Raoof M. and Kraincanic I. (1995) ‘Behavior of Large Diameter Wire Ropes’, Int. J. of Offshore and Polar Engineering, v.6, N3, pp.266-272.

- Raoof M. and Kraincanic I. (1995) ‘Recovery length in multilayered spiral strands’, ASCE, J. Eng. Mech., 121(7), pp.795-800.

- Raoof M. and Kraincanic I. (1995) ‘Recovery Length in Multi-layers Spiral Strands’, J. of Strain Analysis, Inst. of Mechanical Engineers, v.30, N3, pp.217-226.

- Raoof M. (1995) ‘Prediction of Axial Fatigue-Life of spiral Strands’, in Structural Steel, Shanmugan N.E. and Choo Y.S. (eds.), Pergamon, v.1, pp.391-397.

- Raoof M. (1995) ‘Structural Damping in Spiral Strands’, Proc. of the Second European Conf. on Flexible Pipes, Umbilical and Marine Cables Structural Mechanics and Testing, MARINFLEX 95, organized by the University College, London, M.H.Patel and J.A.Witz (eds.), Bentham Press, London, pp.1-26, ISBN 1-874612-24-2.

- Raoof M. (1996) ‘Axial Fatigue Life prediction of Bridge Cables’, Proc. of the Third Int. Conf. on Bridge Management, Inspection, Assessment and Repair, J.E. Harding, G.A.R. Parke, and M.J. Ryall (eds.), E. & F.N. Spon, University of Surrey, Guildform, Surrey, U.K., pp.523-531, ISBN 0 419 212108.

- Raoof M. (1996) ‘Effect of Lay Angle on various characteristics of Spiral Strands’, Int. J. of Offshore and Polar Engineering, v.7, N1, pp.54-62.

- Raoof M. and Kraincanic I. (1996) ‘Characteristics of Locked Coil Cables Under Coupled Axial/Torsional Loading’, Proc. of The 6th International Offshore and Polar Engineering Conference, Chung J.S., Sayed M., Hobbs R.E. and Yoerger D.R. (eds.), Los Angeles, California, USA, v.II, pp.197-203.

- Raoof M. and Kraincanic I. (1996) ‘Prediction of Axial Hysteresis in Locked – Coil Ropes’, J. of Strain Analysis, Inst. of Mechanical Engineers, v.31, N5, pp.341-351.

- Raoof M. and Kraincanic I. (1995) ‘Simple Derivation of the Stiffness Matrix for Axial/Torsional Coupling of Spiral Strands’, Computers and Structures, v.55, N4, pp.589-600.

- Raoof M. and Alani M. (1997) ‘Axial Fatigue of Spiral Strands in Offshore Platform Applications’, Proc. of the 7th International Offshore and Polar Engineering Conference, Chung J.S., Frederking R.M.W., Saeki H. and Bekker A.T.(eds.), Honolulu, Hawaii, USA, v.II, pp.169-176.

- Raoof M. (1998) ‘Recommendations Regarding Design of Spiral Strands Against Axial Fatigue Failure’, Proc. of The 8th International Offshore and Polar Engineering Conference, Chung, J.S., Frederking, R.M.W., Saeki, H., and Moshagen, H., (eds.), Montreal, Canada, v.II, pp.239-247.

- Raoof M. and Kraincanic I. (1998) ‘Determination of Wire Recovery Length in Steel Cables and its Practical Applications’, Computers and Structures, v.68, N5, pp.445-459.

- Raoof M. (1998) ‘Design S-N Curves for Axial Fatigue of Spiral Strands’, Proc. of the Int. Conf. on Long-Span and High-Rise Structures, Kobe, Japan, organized by International Association for Bridge and Structural Engineering, Zurich, Switzerland, v.79, pp.685-690, ISBN 3-85748-095-5.

- Raoof M. and Kraincanic I. (1998) ‘Prediction of Coupled Axial/Torsional Stiffness Coefficients of Locked Coil Ropes’, Computers and Structures, v.69, N3, pp.305-319.

- Raoof M. (1998) ‘Damping performance of Bridge Cables’, Proc. of The Fifth Pacific Structural Steel Conference (PSSC), D.I. Chang, H.N. Cko, C.B. Yun and S.D.Kim (eds.), Seoul, Korea, v.1, pp.521-526, ISBN 89-950031-6-2.

- Raoof M. (1999) ‘Design of Spiral Strands Against Axial Fatigue’, Int. J. of Offshore and Polar Engineering, v.9, N2, pp.149-157.

- Raoof M., Davies T.J. and Scott C.F. (1999) ‘Coupled Axial/Tensional Response to Impact Loading of Helical Cables’, Proc. of the Third Int. Symp. of Cable Dynamics, University of Trondheim, Trondheim, Norway, pp.25-30.

- Raoof M. and Davies T.J. (1999) ‘Restrained Bending Characteristics of Helical Cables at Terminations’, Proc. of the Third Int. Symp. on Cable Dynamics, University of Trondheim, Norway, pp.31-36.

- Raoof M. and Davies T.J. (2000) ‘Possible Shortcomings of Certain Non-Destructive Monitoring Methods for Bridge Cables’, Proc. of the Fourth Int. Conf. on Bridge Management, M.J. Ryall, G.A.R. Parke and J.E. Harding (eds.), Thomas, Telford, University of Surrey, Guildford, Surrey, U.K., pp.154-161, ISBN 0 7277 2854 7.

- Raoof M., Mazza G., Motsonelidze A. and Abuladze V. (2000) ‘Parametric Studies for Investigating Numerical Behavior of Finite/Boundary Elements in the Zones of High Stress Gradients’, Transactions of the Int. Symp. on Problems of Design, Construction and Operation of Hydraulic Structures, Georgian Technical University, Tbilisi, Georgia, pp.37-44, ISBN 99928-0-088-7.

- Raoof M. and Davies T.J. (2002) ‘Simple Determination of Wire Rope Axial Stiffness’, Proc. of the 3rd European Conf. on Steel Structures. A. Lamas and L.S. da Silva (eds.), v.1, Coimbra, Portugal, pp.291-300, ISBN 972-9837-3-5.

- Raoof M. and Davies T.J. (2002) ‘Influence of Variations in the Axial Stiffness of Steel Cables on Vertical Deflections of Cable Trusses’, Proc. of The 3rd European Conf. on Steel Structures, A. Lamas and L.S. Da Silva (eds.), v.1, Coimbra, Portugal, pp.301-310, ISBN 972-98376-3-5.

- Raoof M. and Davies T.J. ‘Experimental Determination of the Spiral Strand’s Bending Stiffness’, submitted to the J. of Strain Analysis, Inst. of Mechanical Engineers.

- Raoof M. (2003) ‘A New S-N Curve for the Restrained Bending Fatigue Design of Bridge Cables’, provisionally accepted for inclusion in the Proc. of the 20th National Conf. on Steel Structures and Bridges, Czech Technical University, Prague, Czech Republic.

- Raoof M. and Davies T.J. (2004) “Determination of the bending stiffness for a spiral strand”, J. Strain Analysis, v.30, pp.1-13.

- Rawlin C.B., ‘Transmission Line Reference Book’, Wind-induced conductor motion, Chapter 2, EPRI, California.

- Samras R.K., Skop R.A. and Milburn D.A. (1974) ‘Analysis of coupled extensional torsional oscillations in wire rope’, J. Eng. Ind., 96, pp.1130-1135.

- Sathikh S. and Chari R.T. (1979) ‘Analytical Derivation of Fatigue Damage Criterion for ACSR Conductors’, Proc. of the IEEE, v.67, N2.

- Sathikh S. (1989) ‘Effect of inter-wire friction on transverse vibration of helically stranded cable’, in Proc. ASME Des. Tech. Conf., Montreal PQ, Canada, ASME, DE. v.18-4, pp.147-153.

- Sathikh S (1990) ‘Discussion of: bending and torsional loading of a strand with friction’, ASCE, J. Eng. Mech., 117(10), pp.2454-2455.

- Sathikh S., Jeya Kumar and Jebaraj C. (1996) ‘Discussion of: A general formulation of the theories of wire ropes’, J. Appl. Mech., 63, pp.1053-1054.

- Sathikh S., Moorthy M.B.K. and Krishnan M. (1996) ‘Symmetric linear elastic model for helical wire stands under axisym. loads’, J. Strain Anal. Eng. Des., 31(5), pp.389-399.

- Sathikh S. and Parthasarathy N.S. (1988) ‘Discussion of: Internal friction due to wire twist in bent cable’, ASCE, J. Eng. Mech., 114(4), pp.727-730.

- Sathikh S. and Parthasarathy N.S. (1989) ‘Effect of contact friction on bending stiffness and slip damping of stranded cable’, in Proc. Nat. Conf. Indust. Trib., Trivandrum, India, Indian Space Res. Org, 1, 11-1-11.6.

- Scanlon R.H. and Swart R.L. (1968) ‘Bending stiffness and strain in stranded cables’, IEEE Winter Power Meeting, New York, Paper No 68-CP-43-PWR PP 9.

- Seppa T. (1971) ‘Self damping measurements and energy balance of ACSR Drake’, IEEE Winter Power Meeting, New York, Paper No 71-CP-161-PWR, PP 8.

- Scalzi J.B. and McGrath W.K. (1971) ‘Mechanical Properties of structural cables’ J. Sturct. Div., ASCE, pp.2837-2844.

- Smith H.L., Stonesiter F.K. and Seibert E.R. (1981) ‘Increased fatigue life of wire rope through periodic overloads’, paper 3256, presented at the may 1981, 10th Annual Offshore Tech Conf. Held at Houston, Tex.

- Starkey W.L. and Cress H.A. (1959) ‘An Analysis of critical stress and mode of failure of a wire rope’, ASME, J. Eng. Ind., pp.P307-316.

- Spain B. (1957) ‘Analytical conics’, Paragon Press, N.Y.

- Seely F.B. and Smith J.O. (1966) ‘Advanced Mechanics of materials’, John Wiley and Sons, Inc., N.Y.

- Shelly P.D. (1974) ‘An analysis of tail rope behavior’, The South African Mech. Engr., 24, pp.310-327.

- Sackfield and Truman (2004) “Some analytical results for plane contact problems”, ASME, J. Strain Anal. Eng., v.39, N4, pp.329-338.

- Timoshenko S. (1956)’Strength of Materials: Part II’, Van Nostrand, New York.

- Timoshenko S. and Goodier J.N. (1951) ‘Theory of Elasticity’, McGraw-Hill, pp.372-382.

- Truss K.J. and Yaskoff F. ‘Study of electrical conductor vibration dampers by means of forced excitation’, Progress report 2, Alcan Research and development limited, Kingston.

- Utting W.S. (1994a) ‘Survey of the literature on the behavior of steel wire ropes- Part I’, Wire Ind., pp.633-635.

- Utting W.S. (1994b) ‘Survey of literature on the behavior of steel wire ropes – part II’, Wire Ind., pp.746-748.

- Utting W.S. (1995) ‘Survey of the literature on the behavior of steel wire ropes – part III’, Wire Ind., pp.269-270.

- Utting W.S. and Jones N. (1984) ‘Survey of literature on the behavior of wire ropes’, Wire Ind., pp.623-629.

- Utting W.S. and Jones N. (1985) ‘Tensile testing of a wire rope strand’, J. Strain Anal. Eng. Des., 20(3), pp.151-164.

- Utting W.S. and Jones N. (1987a), ‘Response of wire rope strands to axial tensile loads. Part I, Experimental result and theoretical predictions’, Int. J. Mech. Sci., 29(9), pp.605-619.

- Utting W.S. and Jones N. (1987b) ‘Response of wire rope strands to axial tensile loads, Part II, Comparison of experimental results and theoretical predictions’. Int. J. Mech. Sci., 29(9), pp.621-636.

- Utting W.S. and Jones N. (1988) ‘Axial – torsional interactions and wire deformation in 19-wire strand’. J. Strain Anal. Eng. Des., 23(2), pp.79-86.

- Velinsky S.A. (1981) ‘Analysis of wire ropes with complex cross sections’, PhD thesis, Univ. of Illinois, Urbana II.

- Velinsky S.A. (1985) ‘Analysis of fiber core wire rope’, J. Energy Res. Tech., v.107, pp.388-393.

- Velinski S.A. (1988) Design and mechanics of multi-lay wire strands. J. Mechanisms Transmissions and Automation in Des., 110(2), pp.152-160.

- Velinsky S.A., Anderson G.L. and Costello G.A. (1984) ‘Wire rope with complex cross sections’, ASCE J. Eng. Mech., 110(3), pp.380-391.

- Vinogradov O.G. and Atatekin I.S. (1986) ‘Internal friction due to wire twist in bent cable’, ASCE J. Eng. Mech., 112(9), pp.859-873.

- Wahl A.M. (1944) ‘Mechanical springs’ First Edition, Pen Ton Publishing Company, Cleveland, Ohio.

- Winter M.H., Durelli J.F., Guidoin R., Cardou A., Laroche G., Fiset M., Guillot M. (1994) ‘Prosthesis oculaires en PMMA quell(s) procede(s) de polymerization faut it privillegier. Comptes rendus des 4emes Journees de I’Institute Europeen des Biomateriauz et de Microchirurgie de Nancy (I.E.B.M.), Nancy, France.

- Wempner G. (1981) ‘Mechanics of solids with applications to thin bodies’, Sijthoff & Noordhoff.

- Wire rope Handbook (1971) St.Joseph, Mo: Leschen Wire Rope Company.

- ‘Yellow strand wire rope’ Handbook, Broderick and Bascom rope company, St. Louis, Miss.

- Yu A. (1952) ‘Vibration damping of stranded cables’, Proc. Soc. Ex. Stress Anal., 9, PP 141-158.

- Yuen W.Y. (1975) ‘Contact problems in wire ropes’, a final year project/report, Mech.Engg.Dept. Univ of New Castle N.S.W. Australia.

- Zhou Z.R., Cardou A., Goudreau S., Fiset M. (1994) ‘Fretting patterns in conductor clamp contact zone’, Fatigue and Fract. of Eng. Mat & Struct, v.17, N6, pp.661-669.

- Zhou Z.R., Cardou A., Fiset M. and Goudreau S. (1994) ‘Fretting fatigue in electrical transmission line’, Wear, v.173, pp.179-188.

- Zhou Z.R., Cardou A., Goudreau S., Fiset M., Vincent L. (1996) ‘Fretting cracking and its prevention; application in transmission line fatigue’, Comptes rendus, MAT-TEC 96, Paris Marne la Vale, France, pp.269-280.

- Zhou Z.R., Goudreau S., Fiset M. and Cardou A. (1995) ‘Single wire fretting fatigue tests for electrical conductor bending fatigue evaluation’, 10th Conf. on Wear of Materials (WOM), Boston, v.181-183, pp.537-543.

- Zemke W.P. (1976) ‘Modeling Technology for bundled power transmission lines’, Ph.D. thesis, Iowa. Sal. Uiv.

- Zhadnov G.P. (1955) ‘Bending Stresses in Steel Wire Ropes’, Nauchnye Trudy Kharkov, Gornogo Inst., v.2, pp.127-135.

- Zhou Z.R., Cardou A., Goudreau S., Fiset M. (1996) ‘Fundamental investigations of electrical conductor fretting fatigue’, Tribology International, v.29, N3, pp.221-232.

- Zhou Z.R., Fiset, M., Cardou A., Cloutier L. et Goudreau S. (1995) ‘Effect of lubricant in electrical conductor fretting fatigue’, Wear, v.189, pp.51-57.

- Zhu Z.H. and Meguid S.A. (2006) “Elastodynamic Analysis of Low Tension Cables Using a New Curved Beam Element”, Int. J. of Solids and Structures, v.43, N6, pp.1490-1504.

- Zhu Z.H. and Meguid S.A. (2007) “Nonlinear FE-based investigation of flexural damping of slacking wire cables”, Int. J. of Solids and Structures, v.44, N16, pp.5122-5132

Поступила в редакцию 13 июля 2007 года.